CẤU TRÚC VÀ TÍNH CHẤT QUANG CỦA VẬT LIỆU ZIRCONIUM(OXY)NITRIDE TỔNG HỢP TỪ HẠT NANO ZIRCONIUM DIOXIDE

Nguyễn Thị Minh Uyên1, Lê Trần Phương Thảo1, Hoàng Thị Hằng3, Phạm Quỳnh Nhi1, Lê Thị Bích Tuyền1, Đặng Bùi Nhật Lê2, Văn Thị Thùy Trang3, Lê Thị Ngọc Loan*3
1 Khoa Sư phạm, Trường Đại học Quy Nhơn
2Khoa Khoa học và kỹ thuật vật liệu, Trường Đại học Phenikaa
3Khoa Khoa học Tự nhiên, Trường Đại học Quy Nhơn 

*Tác giả liên hệ chính. Email: lethingocloan@qnu.edu.vn

TÓM TẮT

Trong những năm gần đây, việc sử dụng thiết bị thu nhiệt năng mặt trời đang ngày càng gia tăng vì đây là một phương pháp trực tiếp và hiệu quả để biến năng lượng mặt trời thành các nguồn năng lượng có thể sử dụng được. Trong xu hướng này, các nghiên cứu tập trung vào việc phát triển cấu trúc nano của các nitride kim loại chuyển tiếp và oxynitride kim loại, nhằm tối đa hóa khả năng thu năng lượng từ mặt trời. Trong nghiên cứu này, chúng tôi đã thành công trong việc tổng hợp vật liệu Zr(O)N để sử dụng trong quá trình chuyển đổi năng lượng quang nhiệt. Quá trình này bao gồm xử lý ZrO2 trong môi trường NH3 ở nhiệt độ cao. Để xác định đặc điểm cấu trúc hình thái và tính chất của các vật liệu này, chúng tôi đã sử dụng kỹ thuật nhiễu xạ tia X (XRD), kính hiển vi điện tử quét (SEM) và phân tích phổ phản xạ khuếch tán tử ngoại khả kiến -(UV-Vis DRS). Các kết quả cho thấy rằng pha tinh thể ZrN bắt đầu hình thành từ nhiệt độ 1150oC. Các vật liệu ZrN/Zr(O)N có khả năng lớn trong việc hấp thụ năng lượng mặt trời và tạo ra nhiệt một cách hiệu quả. Những kết quả này cũng chứng minh rằng ZrN/Zr(O)N có thể được tổng hợp thông qua một phương pháp đơn giản và có tiềm năng lớn trong các ứng dụng chuyển hóa năng lương quang-nhiệt.
Từ khóa: ZrO2 nanoparticles, ZrN, vật liệu quang nhiệt.
STRUCTURAL AND OPTICAL CHARACTERIZATION OF ZIRCONIUM(OXY)NITRIDE SYNTHESIZED FROM ZIRCONIUM DIOXIDE NANOPARTICLES 
Nguyen Thi Minh Uyen1, Le Tran Phuong Thao1, Hoang Thi Hang3, Pham Quynh Nhi1, Le Thi Bich Tuyen1, Dang Bui Nhat Le2, Van Thi Thuy Trang3, Le Thi Ngoc Loan3* 
1Faculty of Pedagogy, Quy Nhon University 
2Faculty of Materials Science and Engineering, Phenikaa University, Yen Nghia, Ha-Dong, Hanoi
3Faculty of Natural Sciences, Quy Nhon University 
*Corresponding. Email: lethingocloan@qnu.edu.vn
ABSTRACT 
In recent years, there has been a growing focus on solar thermal collectors as they offer a direct and efficient means of converting solar energy into usable forms. In line with this, significant attention has been directed towards advancing transition metal nitride and metal oxynitride nanostructures for solar-thermal collectors to maximize solar energy harvesting. In this study, we have successfully synthesized ZrN materials for photothermal energy conversion. The process involved treating ZrO2 in NH3 at high temperatures, resulting in the creation of nanoparticles with promising properties. To characterize the materials, we conducted thorough investigations using X-ray diffraction (XRD), scanning electron microscopy (SEM), and ultraviolet-visible diffuse reflectance spectroscopy (UV-Vis DRS). The findings indicate that the ZrN crystalline phase initiates its formation at 1150°C. The ZrN/Zr(O)N materials possess a robust capacity for absorbing solar energy and efficiently producing heat. Furthermore, these outcomes highlight the feasibility of synthesizing ZrN/Zr(O)N through a straightforward approach, underscoring their significant potential for applications in photothermal conversion.
Keywords: ZrO2 nanoparticles, ZrN, zirconium(oxy)nitride, photothermal energy conversion. 
1. INTRODUCTION
In recent times, there has been a notable increase in the exploration of group IVB transition-metal nitrides, as opposed to noble metals like Au and Ag, to broaden the scope of plasmonic applications and deepen our understanding of light-matter interactions [1]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1002/adma.201205076","ISSN":"09359648","PMID":"23674224","abstract":"Materials research plays a vital role in transforming breakthrough scientific ideas into next-generation technology. Similar to the way silicon revolutionized the microelectronics industry, the proper materials can greatly impact the field of plasmonics and metamaterials. Currently, research in plasmonics and metamaterials lacks good material building blocks in order to realize useful devices. Such devices suffer from many drawbacks arising from the undesirable properties of their material building blocks, especially metals. There are many materials, other than conventional metallic components such as gold and silver, that exhibit metallic properties and provide advantages in device performance, design flexibility, fabrication, integration, and tunability. This review explores different material classes for plasmonic and metamaterial applications, such as conventional semiconductors, transparent conducting oxides, perovskite oxides, metal nitrides, silicides, germanides, and 2D materials such as graphene. This review provides a summary of the recent developments in the search for better plasmonic materials and an outlook of further research directions. © 2013 WILEY-VCH Verlag GmbH & Co. KGaA, Weinheim.","author":[{"dropping-particle":"V.","family":"Naik","given":"Gururaj","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Shalaev","given":"Vladimir M.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Boltasseva","given":"Alexandra","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Advanced Materials","id":"ITEM-1","issue":"24","issued":{"date-parts":[["2013"]]},"page":"3264-3294","title":"Alternative plasmonic materials: Beyond gold and silver","type":"article-journal","volume":"25"},"uris":["http://www.mendeley.com/documents/?uuid=c269f444-fb11-4c9a-adeb-a672a5e2efd6"]}],"mendeley":{"formattedCitation":"[2]","plainTextFormattedCitation":"[2]","previouslyFormattedCitation":"[2]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[2]. This shift has the potential to revolutionize core technologies in fields such as telecommunications, computing, efficient solar harvesting, solid-state lighting, photochemistry, photo- and bio-sensing, diagnostics, and therapeutics [3][4]. Among these materials, titanium nitride (TiN) has garnered significant interest. However, zirconium nitride (ZrN) holds particular importance due to its distinct physical properties, including excellent anti-corrosion characteristics and a high melting point[5]. Importantly, ZrN exhibits a zero crossover wavelength within the visible spectrum, similar to Au, which grants them plasmonic properties in the visible and near-infrared regions [3]. This feature enhances their ability to absorb sunlight and convert it into heat, making them highly suitable for solar light harvesting applications.[6]. This feature enhances their ability to absorb sunlight and convert it into heat, making them highly suitable for solar light harvesting applications.
There are several methods to sysnthesize ZrN, including high energy ball-milling elemental powders of Zr under nitrogen gas-flow at room temperature [7], magnesium thermal reduction process [8], nonthermal plasma reactor [9],  using exothermal reactions initiated by microwave radiation [10], metalorganic

chemical vapor deposition [11][12]. Among these approaches, the reduction-nitridation of zirconium oxide (ZrO2) is frequently employed for the synthesis of zirconium nitride. This method involves the direct nitriding of ZrO2 using ammonia gas at elevated temperatures [13]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1021/cm00043a010","ISSN":"15205002","abstract":"Thermodynamic calculations were performed using the SOLGASMIX-PV computer program to predict the possibility of converting zirconia to zirconium nitride by thermal nitridation in the presence of methane and ammonia. Conversion diagrams were constructed for the ZrO2- NH3-CH4 system over a range of reaction conditions such as temperature, total system pressure, and reagent concentrations. Formation of pure ZrN phase was predicted in the range 1800–2000 K and total system pressures of 0.1–1.0 atm. It is shown experimentally, in the present work, that zirconium nitride can indeed be synthesized by thermal nitridation of zirconia using ammonia and methane at a reaction temperature much lower than that predicted by thermodynamic considerations alone. In addition, no deposition of carbon was observed at the lower temperatures employed during synthesis. Low pressure together with the introduction of excess hydrogen favors the conversion of zirconia to zirconium nitride as well as decrease the reaction temperature for conversion to take place. © 1994, American Chemical Society. All rights reserved.","author":[{"dropping-particle":"","family":"Tan","given":"Beng Jit","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Xiao","given":"Youming","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Galasso","given":"Francis S.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Suib","given":"Steven L.","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Chemistry of Materials","id":"ITEM-1","issue":"7","issued":{"date-parts":[["1994"]]},"page":"918-926","title":"Thermodynamic Analysis and Synthesis of Zirconium Nitride by Thermal Nitridation of Sol-Gel Zirconium Oxide","type":"article-journal","volume":"6"},"uris":["http://www.mendeley.com/documents/?uuid=1fb6b535-198a-41d0-97a5-59982e9e3d85"]}],"mendeley":{"formattedCitation":"[14]","plainTextFormattedCitation":"[14]","previouslyFormattedCitation":"[14]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[14]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1134/S0020168519130016","ISBN":"0020168519","author":[{"dropping-particle":"","family":"Chernyavskii","given":"A S","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Inorganic Materials","id":"ITEM-1","issue":"13","issued":{"date-parts":[["2019"]]},"page":"1303-1327","title":"Synthesis of Ceramics Based on Titanium , Zirconium , and Hafnium Nitrides","type":"article-journal","volume":"55"},"uris":["http://www.mendeley.com/documents/?uuid=ff797790-4e3e-4839-8ebf-be06d74d71a1"]}],"mendeley":{"formattedCitation":"[12]","plainTextFormattedCitation":"[12]","previouslyFormattedCitation":"[12]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[12]. 
Zirconium Nitride (ZrN) possesses distinctive properties, including a high melting point (2952 oC) and hardness ((22.7±1.7 GPa), strong covalent Zr-N bonding and excellent chemical resistance, and stability, making it highly suitable for applications as coatings and protective layers [15]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1016/j.apsusc.2017.06.273","ISSN":"01694332","abstract":"Coatings of single-layer ZrN, bilayer and multilayer ZrN/ZrO 2 were deposited onto 304 stainless steel using a multi-arc ion plating technique, and their corrosion properties were tested in various solutions of 3.5 wt% sodium chloride (NaCl), 10 wt% and 20 wt% hydrochloric (HCl) acids, respectively.Results showed that the single-layer ZrN coating resisted the corrosion in the HCl acid with a concentration of 10 wt%, and the multilayer ZrN/ZrO 2 coating acted as an effective protective layer in 20 wt% HCl solution. Polarization curve of the bilayer ZrN/ZrO 2 coated specimens showed the lowest corrosion current density in 3.5 wt% NaCl and 20 wt% HCl solutions. However after polarization tests, the bilayer coating showed severe delamination after exposed in air, due to the large coating stress and brittleness of oxide ceramic layer. The multilayer ZrN/ZrO 2 coating exhibited similar corrosion potentials and corrosion current densities compared with those of the bilayer coating. However, there was hardly any microscopic failure observed on the surfaces of the multilayer coatings after tested in all chloride solutions, which is attributed to the combined effects including improvement in coating toughness due to the multilayer design and ZrN sub-layer, reduced coating stress, and good corrosion resistance from the ZrO 2 sub layer.","author":[{"dropping-particle":"","family":"Lei","given":"Zhefeng","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Zhang","given":"Qingqing","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Zhu","given":"Xiaodong","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Ma","given":"Dayan","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Ma","given":"Fei","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Song","given":"Zhongxiao","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Fu","given":"Yong Qing","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Applied Surface Science","id":"ITEM-1","issued":{"date-parts":[["2018"]]},"page":"170-176","publisher":"Elsevier B.V.","title":"Corrosion performance of ZrN/ZrO2 multilayer coatings deposited on 304 stainless steel using multi-arc ion plating","type":"article-journal","volume":"431"},"uris":["http://www.mendeley.com/documents/?uuid=97a05563-a0b1-4cb7-b65a-04dd8fb51561"]}],"mendeley":{"formattedCitation":"[16]","plainTextFormattedCitation":"[16]","previouslyFormattedCitation":"[16]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[16][17]. Recently, ZrN has garnered attention as an excellent material for electrodes in energy storage and conversion [18], owing to its exceptional electrical conductivity, mobility, and impressive electrochemical performance[19][4][20]. Moreover, ZrN has emerged as a promising alternative plasmonic material, finding diverse applications in solar cells [21], solar light harvesting [22], and solar to heat energy conversion [23][24]. Its unique properties make it a valuable candidate in these solar-related technologies. Furthermore, zirconium oxynitride, similar to zirconium nitride, has piqued special interest as a material for solar-thermal collectors. This interest is due to its remarkable solar absorptance and thermal stability [25][9][24]. Thus, both ZrN and zirconium oxynitride exhibit great potential in advancing various applications related to energy conversion and utilization.
In this study, a straightforward approach was introduced to produce zirconium(oxy)nitride nanoparticles through the reduction-nitridation process of zirconium oxide nanoparticles (ZrO2 NPs) in NH3 gas at elevated temperatures. SEM images illustrated that average particles increased during nitridation process. Notably, the results revealed the formation of cubic ZrN phase at 1150°C, and the materials exhibited strong and broad absorption spanning from the visible to near-infrared region (~300 – 2000 nm). Furthermore, the potential of the synthesized nanoparticles in solar-thermal energy conversion was also assessed. 

2. Experimental

2.1.Chemicals: the raw materials used in this study including zirconium dioxide (ZrO2, 99.95%), zirconium nitride (ZrN, 99.9%),  ammonia and nitrogen gas (NH3, H2, > 99.9%) were supplied from Aladdin Reagent Co., Ltd., China.
2.2. NH3 treatment of ZrO2 nano particles
Initially, 8 mg of ZrO2 powder was carefully placed into a ceramic boat, which was then positioned at the center of a quartz-tube furnace using a customized setup. This setup allowed for precise control of temperature, pressure, and gas flow during the experiment. One end of the quartz tube was connected to the gas inlet, with N2 and NH3 gases available. The other end was connected to a mechanical vacuum pump. To begin the process, the quartz tube was evacuated to achieve a vacuum level of 10−3 mbar. Subsequently, the furnace was pre-heated to 300 °C. To eliminate any contaminants, the tube was purged multiple times with N2 gas. Once prepared, the temperature in the furnace was raised either to 1050 or 1150 °C, both at a ramping rate of 5 °C min−1. After the desired temperature was stabilized, pure ammonia gas was introduced into the furnace at a flow rate of 400 sccm for a duration of 1.5 hours. Following this, the furnace was gradually cooled down to 100 °C in an NH3 environment and further to room temperature in N2 before unloading the sample. 
2.3. Material characterization 

The crystalline structure of the obtained samples was studied by powder X-ray diffraction (XRD) employing an X-ray diffractometer (Brucker Phaser, D2) using Cu Kα irradiation (λ = 0.154 nm). The surface morphology of the synthesized materials was characterized by scanning electron microscopy (SEM) using a HITACHI S-4800 microscope. UV-Vis absorption spectra were measured using a Shimadzu 2600 UV-visible spectrometer.

2.4. Photothermal materials study

For each experimental run, 0.8 g of PVP (Polyvinylpyrrolidone) and 9.5 mL of DMF (N,N-Dimethylformamide) were combined in a 100 mL glass beaker and stirred for a period of 4 hours. Subsequently, 0.01 g of ZrO2 1150 nanoparticles was added to the mixture and dispersed with sonication for 10 minutes. The resulting ZrO2 1150 nanoparticle suspension was then used to create thin layers on glass slides (2 cm x 2 cm) through the spin-coating method, spinning at 1500 rpm for 60 seconds.

To evaluate the solar-thermal energy conversion performance of the prepared samples, a custom-made closed metal chamber made of steel was utilized. The metal chamber was insulated with fiber glass material to minimize heat loss. The prepared samples were placed at the center of this chamber and exposed to sunlight irradiation. The temperature of the ZrO2 1150 layer was monitored using a K-type temperature probe. Additionally, temperature measurements inside the chamber and the ambient air outside were recorded using mercury temperature meters. The photon flux of sunlight was measured using a luminous flux meter from China. Throughout the experiments, data was recorded at 10-minute intervals to analyze the performance of the samples..
3. Results and discussion
The XRD patterns of the ZrO2 NPs before and after the NH3 treatment at 1050 and 1150 oC (sample ZrO2 1050 and ZrO2 1150) are presented in Fig. 1. In the case of ZrO2 nanoparticles (referred to as ZrO2 TM), all observed diffraction peaks corresponding to monoclinic (m) and tetragonal (t) crystal structure phases were accurately matched with standard data of ZrO2 (PDF Card - 00-036-0420 and PDF Card - 00-042-1164, respectively) [26]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1016/j.ultsonch.2014.10.004","ISSN":"1350-4177","author":[{"dropping-particle":"","family":"Manoharan","given":"Divinah","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Loganathan","given":"Aswaghosh","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Kurapati","given":"Vishista","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Nesamony","given":"Victor Jaya","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Ultrasonics - Sonochemistry","id":"ITEM-1","issued":{"date-parts":[["2015"]]},"page":"174-184","publisher":"Elsevier B.V.","title":"Ultrasonics Sonochemistry Unique sharp photoluminescence of size-controlled sonochemically synthesized zirconia nanoparticles","type":"article-journal","volume":"23"},"uris":["http://www.mendeley.com/documents/?uuid=71d40c2b-f5e9-4b4e-832a-12cf6ddf88a7","http://www.mendeley.com/documents/?uuid=53fa1a67-620f-4921-a318-0bfd8334145f"]}],"mendeley":{"formattedCitation":"[27]","plainTextFormattedCitation":"[27]","previouslyFormattedCitation":"[27]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[27]. This result also indicates high purity of ZrO2 TM (red trace).

	[image: image1.png]Intensity (a.u)

Zr0, 1150

Zr021050
‘LA-_AAAAA A A EA

Nt ZrOTM

(111)5 ZrN CUbIC

(200) (220) i (31 1)

20 25 30 35 40 45 50 55 60 65 70

2 Theta (degree)





	Fig. 1. XRD diffraction patterns of ZrO2 precusor and ZrO2 after annealing in NH3 at 1050 and 1150 oC


Upon NH3 treatment of ZrO2 at 1050°C, the peaks related to the monoclinic (m) phase of ZrO2 nearly vanish, while most of those corresponding to the tetragonal ZrO2 remain, e.g., at 30o, 36o and 61.5o. In addition, the peaks of Zr2ON2 appear at 21o, 30o, 35o, 37.5o and 51o. This observation is in good agreement with previous report [28]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1063/1.2927494","ISSN":"00218979","abstract":"This work is devoted to the investigation of decorative zirconium oxynitride, Zr Ox Ny, films prepared by dc reactive magnetron sputtering, using a 17:3 nitrogen-to-oxygen-ratio gas mixture. The color of the films changed from metallic-like, very bright yellow pale, and golden yellow, for low gas mixture flows [from 0 to about 9 SCCM (SCCM denotes cubic centimeter per minute at STP)] to red brownish for intermediate gas flows (values up to 12 SCCM). Associated to this color change there is a significant decrease of brightness. With further increase of the reactive gas flow, the color of the samples changed from red brownish to dark blue (samples prepared with 13 and 14 SCCM). The films deposited with gas flows above 14 SCCM showed only apparent colorations due to interference effects. This change in optical behavior from opaque to transparent (characteristic of a transition from metallic to insulating-type materials), promoted by the change in gas flow values, revealed that significant changes were occurring in the film structure and electronic properties, thus opening new potential applications for the films, beyond those of purely decorative ones. Taking this into account, the electrical behavior of the films was investigated as a function of the reactive gas flow and correlated with the observed chemical, electronic, and structural features. The variations in composition disclosed the existence of four different zones, which were correlated to different crystalline structures. For the so-called zone I, x-ray diffraction revealed the development of films with a B1 NaCl face-centered cubic zirconium nitride-type phase, with some texture changes. Increasing the reactive gas flow, the structure of the films is that of a poorly crystallized overstoichiometric nitride phase, which may be similar to that of Zr3 N4, but with some probable oxygen inclusions within nitrogen positions. This region was characterized as zone II. Zone III was indexed as an oxynitride-type phase, similar to that of γ- Zr2 O N2 with some oxygen atoms occupying some of the nitrogen positions. Finally, occurring at the highest flow rates, zone IV was assigned to a Zr O2 monoclinic-type structure. The compositionstructure variations were consistent with the chemical bonding analysis carried out by x-ray photoelectron spectroscopy, which showed oxygen doping in both Zr3 N4 - and ZrN-type grown films. The electronic properties of the films exhibited significant changes from zone to zone.…","author":[{"dropping-particle":"","family":"Carvalho","given":"P.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Chapṕ","given":"J. M.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Cunha","given":"L.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Lanceros-Ḿndez","given":"S.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Alpuim","given":"P.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Vaz","given":"F.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Alves","given":"E.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Rousselot","given":"C.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Espinós","given":"J. P.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"González-Elipe","given":"A. R.","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Journal of Applied Physics","id":"ITEM-1","issue":"10","issued":{"date-parts":[["2008"]]},"title":"Influence of the chemical and electronic structure on the electrical behavior of zirconium oxynitride films","type":"article-journal","volume":"103"},"uris":["http://www.mendeley.com/documents/?uuid=bc400683-8b70-4e26-8212-7e1520ab60f7"]}],"mendeley":{"formattedCitation":"[29]","plainTextFormattedCitation":"[29]","previouslyFormattedCitation":"[29]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[29] (pink trace). Furthermore, at the higher temperature of 1150°C, the treatment results in the appearance of new peaks at 34°, 39°, 57°, and 68°, corresponding to diffraction planes of the (111), (200), (200), and (311) atomic planes of the face-centered cubic (FCC) structure of ZrN (PDF Card - 00-031-1493) [16]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1166/jnn.2019.16119","author":[{"dropping-particle":"","family":"Yin","given":"Wenyan","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Wang","given":"Qiang","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Journal of Nanoscience and Nanotechnology","id":"ITEM-1","issue":"June","issued":{"date-parts":[["2019"]]},"page":"3319–3325","title":"Feasibility of Biological Applications for Zirconium Nitride Powders Synthesized by Gas – Solid Elemental Combination Method","type":"article-journal","volume":"19"},"uris":["http://www.mendeley.com/documents/?uuid=5822cee3-914b-4c3f-93c1-58a99adc502c","http://www.mendeley.com/documents/?uuid=875d3009-6f47-4e18-9cf4-ee557b092335"]}],"mendeley":{"formattedCitation":"[30]","plainTextFormattedCitation":"[30]","previouslyFormattedCitation":"[30]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[30]. Interestingly, annealing ZrO2 in NH3 transforms the mixture of monoclinic and tetragonal crystal structure phases into the single phase of t-ZrO2 and initiates a new phase of ZrN.
Figure 2 displays scanning electron microscopy (SEM) images of a representative sample, along with the particle size distribution, which was measured and determined using Digital Micrograph. 
[image: image2.png]d = 137.67:40.30 nm

60 80 100120140 160 180200 220 240
Diameter (nm)

d =206.58:45.90 nm

\ ST
100 150 200 250 300
Diameter (nm)

d=238.03+64.69nm

0
50 100 150 200 250 300 350 400
Diameter (nm)





Figure 2. SEM images and the particle size distribution of (a) ZrO2 TM, as well as ZrO2 after being treated in NH3 at different temperatures: (b) 1050°C, and (c) 1150°C. The color of the powders is also illustrated in the respective insets.
The SEM images present the shapes and sizes of ZrO2 TM nanoparticles (Fig. 2a) and the same nanoparticles after annealing in ammonia at 1050°C (Fig. 2b) and 1150°C (Fig. 2c). In Fig. 2a, ZrO2 TM exhibits a wide variation in particle sizes, with an average diameter of approximately 137.67 ± 40.30 nm, represented by the top red distribution curve. After treatment at 1050°C, the average diameter increases significantly to 206.58 ± 45.90 nm, a nearly 15% increment, as shown by the middle blue distribution. Subsequently, the particle size further grows by about 17% after treatment  NH3 at 1150°C, resulting in an average diameter of about 238.03 ± 64.69 nm, as illustrated in the bottom black curve.

The findings reveal that NH3 treatment at temperatures ranging from 1050 to 1150°C does not significantly impact the surface morphology of the nanoparticles. However, it does induce remarkable changes in both particle size and the appearance of the powder color. These color variations are clearly visible in the optical images within the SEM images, showcasing a gradual shift from white (ZrO2 TM) to dark gray (ZrO2 1050) and ultimately black (ZrO2 1150), which is the typical color of ZrN powder. This color transformation aligns with the light absorption characteristics observed in the following UV-Vis absorption spectra.

To investigate the optical properties of the composites, UV-vis diffuse reflectance spectral analysis was conducted on ZrO2 powder, as well as the ZrO2 samples treated in NH3 at 1050 and 1150°C. The results obtained from the analysis are presented in Fig. 3.
	[image: image3.png]Absorbance

1.4 - "

2,

1.0 - ® 1o

0.8- Zr0, 1150 T 2525 5 35 45 45

0.6- ZrO, 1050

oa

0.2- ngﬂﬂ,k _

0.0 -1+
500 1000 1500

Wavelength (nm)

2000






	Figure 3. UV–Vis absorption spectra of the representative samples and the corresponding band gap  calculations using the Kubelka-Munk method as indicated in the inset.


The UV vis absorption spectrum ZrO2 TM shows a sharp and prominent absorption band with maximum at around 277 nm (4.48 eV in photon energy) which can arise due to the transition between valence band to conduction band [31]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1063/1.2386967","author":[{"dropping-particle":"","family":"Garcia","given":"J C","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Scolfaro","given":"L M","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Lino","given":"A T","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Freire","given":"V N","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Farias","given":"G A","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Journal od Applied Physics","id":"ITEM-1","issued":{"date-parts":[["2006"]]},"page":"104103","title":"Structural , electronic , and optical properties of ZrO2 from ab initio calculations","type":"article-journal","volume":"100"},"uris":["http://www.mendeley.com/documents/?uuid=0f71b1ec-fa5c-48f7-aca3-a1b629c5a27e"]}],"mendeley":{"formattedCitation":"[28]","plainTextFormattedCitation":"[28]","previouslyFormattedCitation":"[28]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[28]. However, this absorption peak for the ZrO2 nanostructure in the UV-region is at lower energy as compared to the previous report on the optical band gap for bulk ZrO2 (5.0 eV) [32]. This indicates that there is still contribution from extrinsic states towards the absorption in this region. Apart from the strong absorption peak, a broad and weak absorption  from visible to near infrared exists. The weak absorption in the visible and near IR region is expected to arise from transitions involving extrinsic states such as surface trap states or defect states or impurities [32]. The direct band gap energy can be determined by Kubelka-Munk method, about 3.7 eV, as indicated by the blue trace in the inset of Fig. 3.
When comparing with pure ZrO2, the absorption spectrum of ZrO2 1050 reveals distinct characteristics. It displays a pronounced absorption peak at 391 nm with an energy gap (Eg) of approximately 2.3 eV, as depicted in the red trace within the inset. Additionally, there's a broad and potent absorption band spanning from the visible to the near-infrared spectrum. The initial absorption can be attributed to the band gap of zirconium oxynitride [28][33][34], while the broad absorption is the result of a continuous depopulation of the d-band and the creation of an energy gap between the valence band and the Fermi level [35]. 
Upon increasing the annealing temperature to 1150°C, a phase transition to ZrN commences from the outer layer of ZrO2 1150 particles, as evidenced by the XRD pattern. This transformation yields a significantly intensified and broadened absorption spectrum over a wide range, extending from the ultraviolet to the near-infrared region. Several factors contribute to this phenomenon, including the plasmonic behavior arising from the metallic content of ZrN/Zr2ON2 [9][36], the presence of oxygen/zirconium vacancies or interstitials  [32]

ADDIN CSL_CITATION {"citationItems":[{"id":"ITEM-1","itemData":{"DOI":"10.1021/cg800711m","ISSN":"15287483","abstract":"Zirconium oxide (ZrO2 or zirconia) nanostructures were synthesized by a hydrothermal route. Surface morphology analysis depicts the formation of various zirconia nanostructures at different synthesis conditions. X-ray diffraction examination demonstrates that the as-synthesized zirconia is of pure monoclinic phase (m-ZrO2). High resolution transmission electron microscopy (HRTEM) further confirms the high crystalline feature of the m-ZrO2 nanostructures. X-ray photoelectron spectroscopy (XPS) core-level spectra of Zr 3d and O 1s for the ZrO2 nanostructures have been studied to understand further the electronic states and chemical environment of the Zr and O atoms in ZrO2 for different synthesis conditions. XPS results also indicate the existence of oxygen defects and zirconia suboxides which affect the structural and optical properties of zirconia nanostructures. The nanostructures show UV-vis absorption band around 290 nm at room temperature. The band gap energy is determined, in the range of 2.5-3.8 eV for zirconia nanostructures synthesized at various conditions. A broad emission band with maximum intensity at around 400 nm is observed in the photoluminescence (PL) spectra of zirconia nanostructures at room temperature depicting the violet emission, which can be attributed to the ionized oxygen vacancy in the material. © 2009 American Chemical Society.","author":[{"dropping-particle":"","family":"Kumari","given":"Latha","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Li","given":"W. Z.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Xu","given":"J. M.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Leblanc","given":"R. M.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Wang","given":"D. Z.","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Li","given":"Yi","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Guo","given":"Haizhong","non-dropping-particle":"","parse-names":false,"suffix":""},{"dropping-particle":"","family":"Zhang","given":"Jiandi","non-dropping-particle":"","parse-names":false,"suffix":""}],"container-title":"Crystal Growth and Design","id":"ITEM-1","issue":"9","issued":{"date-parts":[["2009"]]},"page":"3874-3880","title":"Controlled hydrothermal synthesis of zirconium oxide nanostructures and their optical properties","type":"article-journal","volume":"9"},"uris":["http://www.mendeley.com/documents/?uuid=30cfc3d7-543e-45bf-a9df-df654aeecf79"]}],"mendeley":{"formattedCitation":"[37]","plainTextFormattedCitation":"[37]","previouslyFormattedCitation":"[37]"},"properties":{"noteIndex":0},"schema":"https://github.com/citation-style-language/schema/raw/master/csl-citation.json"}[37] and a diverse distribution of particle sizes, as observed in Figure 2. Notably, the broad plasmon resonance spectrum featuring a central peak around 530 nm and the heightened light absorption within the visible-near infrared range at elevated temperatures hold immense promise for applications in solar light harvesting.
Figure 4 illustrates temperature measurements conducted within a metallic enclosure and on glass coated with ZrO2 1150 nanoparticles. The temperature of the ZrO2 1150-coated glass is depicted as the red trace, the air temperature within the chamber is represented by the black trace, and the photon flux is displayed as the blue trace (transmitted through a chamber window glass with over 90% light transmission). In Figure 4a, temperature measurements taken outdoors in an environment with an ambient air temperature of 26°C are displayed for both inside the chamber and the glass film coated with ZrO2 1150 nanoparticles, all under sunlight illumination.

The outcomes reveal a proportional increase in the temperature of the ZrO2 1150-coated glass with rising photon flux. After a continuous 60-minute exposure to sunlight, the glass coated with ZrO2 1150 nanoparticles reaches a peak temperature of 60°C, presenting a temperature differential (ΔT) of approximately 15°C above the air temperature within the enclosed metal box (around 45°C). These initial findings strongly suggest the potential of zirconium oxynitride as a viable material for applications involving photothermal energy conversion.

	[image: image4.jpg]Temp. (°C)

T T
Ambient Temp. 260C

280

65
(@) I 260
60 _
—" L0 %
55 8
F220 X%
5
50 2
F200 5
45 2
|80 &
o= inside charmper
—B~—Glass coated 20 drops ZrN
404 —o—Photon flux@Outdoor
I 160
r r T . T :
0 10 20 30 40 50 60






	Fig 4. Temperature arising from ZrO2 1150 material under sunlight exposure: the temperature of the ZrO2 1150-coated glass is depicted as the red trace, the air temperature within the chamber is represented by the black trace, and the photon flux is displayed as the blue trace (transmitted through a chamber window glass with over 90% light transmission).


4. Conclusion
In brief, we have illustrated a straightforward method for producing Zirconium(oxy)nitride nanoparticles. These particles display robust and extensive light absorption across a wide spectrum of solar wavelengths, encompassing the UV-vis to infrared range, notably peaking at around 530 nm. We evaluated their ability for photothermal energy conversion by employing a metal chamber setup, where ZrO2-coated glass nanoparticles were tested. The results indicated a significant heat generation, surpassing the surrounding temperature by approximately 30%. This experimentation underscores the promising prospects of utilizing zirconium(oxy)nitride for enhancing solar-to-heat conversion performance.
Acknowledgements

This work is financially supported by the Ministry of Education and Training of Vietnam under the grant number B2022-DQN-04.

References
[1]
A. Lalisse, G. Tessier, J. Plain, and G. Baffou, “Plasmonic efficiencies of nanoparticles made of metal nitrides (TiN, ZrN) compared with gold,” Sci. Rep., 2016,  6, 1–10.

[2]
G. V. Naik, V. M. Shalaev, and A. Boltasseva, “Alternative plasmonic materials: Beyond gold and silver,” Adv. Mater., 2013, 25 (24), 3264–3294.

[3]
U. Guler, V. M. Shalaev, and A. Boltasseva, “Nanoparticle plasmonics : going practical with transition metal nitrides,” Biochem. Pharmacol., 2014, 18 (4), 227–237.

[4]
P. Patsalas, “Zirconium nitride : A viable candidate for photonics and plasmonics?,” Thin Solid Films, 2019, 688, 137438.

[5]
J. Tan, “Thermodynamic Analysis and Synthesis of Zirconium Nitride by Thermal Nitridation of Sol-Gel Zirconium Oxide,” 2000, 7, 918–926.

[6]
U. Guler, V. M. Shalaev, and A. Boltasseva, “Nanoparticle plasmonics : going practical with transition metal nitrides,”  2014, 18 (4), 1–11.

[7]
M. S. El-Eskandarany and A. H. Ashour, “Mechanically induced gas-solid reaction for the synthesis of nanocrystalline ZrN powders and their subsequent consolidations,” J. Alloys Compd., 2000, 313, 1, 224–234.
[8]
Z. Y. Wu et al., “Solid-state synthesis of zirconium nitride and hafnium nitride powders,” J. Ceram. Soc. Japan, 2021, 129 (3), 200–203, 2021.

[9]
S. Exarhos, A. Alvarez-Barragan, E. Aytan, A. A. Balandin, and L. Mangolini, “Plasmonic Core-Shell Zirconium Nitride-Silicon Oxynitride Nanoparticles,” ACS Energy Lett., 2018, 3 (10), 2349–2356.

[10]
R. A. Shishkin and E. S. Maiorova, “Microwave vs Autoclave Synthesis of Nanodisperse ZrN Powder,” Glas. Ceram., 2017, 74 (3), 123–125.

[11]
M. Banerjee et al., “Fabrication of ZrO 2 and ZrN films by metalorganic chemical vapor deposition employing new Zr precursors,” Cryst. Growth Des., 2012, 12(10), 5079–5089.

[12]
A. S. Chernyavskii, “Synthesis of Ceramics Based on Titanium , Zirconium , and Hafnium Nitrides,” Inorg. Mater., 2019, 55 (13), 1303–1327.

[13]
B. Fu and L. Gao, “Synthesis of nanocrystalline zirconium nitride powders by reduction-nitridation of zirconium oxide,” J. Am. Ceram. Soc., 2004, 87 (4), 696–698.

[14]
B. J. Tan, Y. Xiao, F. S. Galasso, and S. L. Suib, “Thermodynamic Analysis and Synthesis of Zirconium Nitride by Thermal Nitridation of Sol-Gel Zirconium Oxide,” Chem. Mater., 1994, 6 (7), 918–926.

[15]
S. K. Kim and V. Van Le, “Surface & Coatings Technology Cathodic arc plasma deposition of nano-multilayered ZrN / AlSiN thin fi lms,” Surf. Coat. Technol., vol. 206, no. 6, pp. 1507–1510, 2011.

[16]
Z. Lei et al., “Corrosion performance of ZrN/ZrO2 multilayer coatings deposited on 304 stainless steel using multi-arc ion plating,” Appl. Surf. Sci., vol. 431, pp. 170–176, 2018.

[17]
Y. Lu, Z. Yuan, H. Shen, X. Huai, and Z. Huang, “High-temperature phase relations of ZrN–ZrO2–Y2O3 ternary system,” J. Adv. Ceram., vol. 7, no. 4, pp. 388–391, 2018.

[18]
T. Boldoo, J. Ham, E. Kim, and H. Cho, “Review of the Photothermal Energy Conversion Performance of Nanofluids, Their Applications, and Recent Advances,” Energies, vol. 13, no. 21, p. 5748, 2020.

[19]
Y. Zhong, X. H. Xia, F. Shi, J. Y. Zhan, J. P. Tu, and H. J. Fan, “Transition metal carbides and nitrides in energy storage and conversion,” Adv. Sci., vol. 3, no. 5, 2015.

[20]
R. W. Harrison and W. E. Lee, “Processing and properties of ZrC, ZrN and ZrCN ceramics: a review,” Adv. Appl. Ceram., vol. 115, no. 5, pp. 294–307, 2016.

[21]
N. Saiprasad, A. Boretti, L. Rosa, and S. Castelletto, “Novel plasmonic materials to improve thin film solar cells efficiency,” Micro+Nano Mater. Devices, Syst., vol. 9668, p. 966847, 2015.

[22]
G. Baffou, F. Cichos, and R. Quidant, “Applications and challenges of thermoplasmonics,” Nat. Mater., vol. 19, no. 9, pp. 946–958, 2020.

[23]
T. L. Thi Le et al., “Titanium nitride nanodonuts synthesized from natural ilmenite ore as a novel and efficient thermoplasmonic material,” Nanomaterials, 2021, 11 (1), 76–87.

[24]
K. Xu, M. Du, L. Hao, J. Mi, Q. Yu, and S. Li, “A review of high-temperature selective abXu, Ke, et al. ‘A Review of High-Temperature Selective Absorbing Coatings for Solar Thermal Applications.’ Journal of Materiomics, 2020, 6 (1), 167–82. 

[25]
K. Ibrahim, H. Taha, M. M. Rahman, H. Kabir, and Z. T. Jiang, “Solar selective performance of metal nitride/oxynitride based magnetron sputtered thin film coatings: A comprehensive review,” J. Opt. (United Kingdom), 2018, 20 (3), 033001.

[26]
P. R. Rauta, P. Manivasakan, V. Rajendran, B. B. Sahu, B. K. Panda, and P. Mohapatra, “Phase transformation of ZrO2 nanoparticles produced from zircon,” Phase Transitions, 2012, 85 (1), 13–26.

[27]
D. Manoharan, A. Loganathan, V. Kurapati, and V. J. Nesamony, “Ultrasonics Sonochemistry Unique sharp photoluminescence of size-controlled sonochemically synthesized zirconia nanoparticles,” Ultrason. - Sonochemistry, 2015, 23, 174–184.

[28]
J. C. Garcia, L. M. Scolfaro, A. T. Lino, V. N. Freire, and G. A. Farias, “Structural , electronic , and optical properties of ZrO2 from ab initio calculations,” J. od Appl. Phys., 2006, 100, 104103.

[29]
P. Carvalho et al., “Influence of the chemical and electronic structure on the electrical behavior of zirconium oxynitride films,” J. Appl. Phys., 2008, 103, 10.

[30]
W. Yin and Q. Wang, “Feasibility of Biological Applications for Zirconium Nitride Powders Synthesized by Gas – Solid Elemental Combination Method,” J. Nanosci. Nanotechnol., 2019, 19, 3319–3325.

[31]
L. Kumari, G. H. Du, W. Z. Li, R. S. Vennila, S. K. Saxena, and D. Z. Wang, “Synthesis, microstructure and optical characterization of zirconium oxide nanostructures,” Ceram. Int., 2009, 35 (6), 2401–2408.

[32]
A. Emeline, G. V. Kataeva, A. S. Litke, A. V. Rudakova, V. K. Ryabchuk, and N. Serpone, “Spectroscopic and photoluminescence studies of a wide band gap insulating material: Powdered and colloidal ZrO2 sols,” Langmuir, 1998, 14 (18), 5011–5022.

[33]
D. I. Bazhanov, A. A. Knizhnik, A. A. Safonov, A. A. Bagatur’yants, M. W. Stoker, and A. A. Korkin, “Structure and electronic properties of zirconium and hafnium nitrides and oxynitrides,” J. Appl. Phys., 2005, 97 (4), 044108.
[34]
T. D. Boyko, A. Zerr, and A. Moewes, “Tuning the Electronic Band Gap of Oxygen-Bearing Cubic Zirconium Nitride,” ACS Appl. Electron. Mater., 2021, 3, 4768−4773.

[35]
P. Carvalho et al., “Optical properties of zirconium oxynitride films: The effect of composition, electronic and crystalline structures,” Appl. Surf. Sci., 2015, 358, 660–669.

[36]
Q. Guo et al., "Plasmonic properties of nonstoichiometric zirconium nitride , oxynitride thin films , and their bilayer structures,” Phys. Rev. Mater., 2021, 5 (6), 65201.

[37]
L. Kumari et al., “Controlled hydrothermal synthesis of zirconium oxide nanostructures and their optical properties,” Cryst. Growth Des., 2009, 9 (9), 3874–3880.

[38]
S. Exarhos, A. A. Barragan, E. Aytan, A. A. Balandin, and L. Mangolini, “Plasmonic Core-Shell Zirconium Nitride – Silicon Oxynitride Nanoparticles,” ACS Energy Lett., 2018, 3 (10), 2349–2356.



Liên hệ: Tên tác giả liên hệ chính
Lê Thị Ngọc Loan, Email: lethingocloan@qnu.edu.vn
1

