CỘNG HOÀ XÃ HỘI CHỦ NGHĨA VIỆT NAM

Độc lập – Tự do – Hạnh phúc

------------***-----------

GIẢI TRÌNH NHẬN XÉT CỦA PHẢN BIỆN 1

BÀI BÁO: SYNTHESIS OF CeO2 AND ITS APPLICATION FOR TREATING ORGANIC DYES IN WATER.

BẢNG*: DANH SÁNH TIẾP THU VÀ SỬA LỖI

| Câu hỏi | Nội dung ban đầu | Nội dung sau khi sửa tiếp thu |
| --- | --- | --- |
| 1- Trên tất cả các giản đồ XRD (Fig. 2, 3, 4, 5) cần chỉ rõ đầy đủ 4 peak có cường độ thấp ở 2theta > 57 độ, cụ thể ứng với các mặt phẳng (202), (400), (331) và (420) theo JCPDS card: 34-0394 của CeO2 | Không có | The peaks located at 2θ = 28.5; 33.1; 47.5; 56.5; 59.1; 70.0; 76.5 and 79.5 correspond to the (111), (200), (220), (311), (222), (400), (331), and (420) crystal planes of CeO2, respectively, according to JCPDS card: 34-03949 |
| Cần cân nhắc bình luận kết quả XRD của Fig.3 | However, at pH 4, the characteristic peak at 2θ = 26° exhibited abroader width compared to other values. This suggests the potential formation of smaller-sized oxide particles. | However, if the pH is low (pH2, pH3), it can break the polymer chains of PVA, reducing the uniform dispersion of metal cations in the network. The appropriate pH here is pH3, pH4. In the next study, pH 4 was chosen. |
| Cân nhắc bình luận XRD sau Fig.4 | Therefore, the characteristic peaks of CeO2 formed were not clear and unstable. At ratios of Ce/AP = 1/3; Ce/AP = 1/9, characteristic peaks were clearly shown | At ratios of Ce/AP = 9/1; Ce/AP = 3/1; Ce/AP = 1/1 of the amount of agent used to form complexes with metal ions were not enough, resulting gels exhibited poor viscosity. When forming gels at Ce/AP = 1/3 and 1/9, it ensured the appropriate amount of gel-forming agent, leading to high viscosity gels. Upon thermal treatment, the products showed increased porosity and more uniform particle sizes. However, as shown in Figure 4, at the Ce/AP = 1/9, the peaks formed were higher and sharper compared to the Ce/AP = 1/3. This may indicate an increase in the crystal size of the obtained material. Therefore, the Ce/AP = 1/3 was chosen for further studies. |
| Về đặc trưng BET, nếu có thể tác giả nên bổ sung "Đường cong hấp phụ-giải hấp phụ N2 ở 77K của vật liệu | Không có | Figure 7 shows the N2 adsorption–desorption isotherms and the pore size distribution plot of the CeO2 samples |

Ngoài ra, cũng đã chỉnh sửa hoàn chỉnh các lỗi chính tả, cập nhật tài liệu tham khảo và một số lỗi khác theo góp ý của phản biện.

Tôi xin trân trọng cảm ơn!

Thay mặt nhóm tác giả

Nguyễn Vũ Ngọc Mai