
Tổng hợp CeO2 và ứng dụng xử lý chất màu hữu cơ trong môi trường nước
TÓM TẮT
Nghiên cứu này tổng hợp vật liệu CeO2 sử dụng hai tác nhân tạo gel là tartaric acid (A) và polyvinyl alcohol (P) bằng phương pháp đốt cháy. Các đặc trưng được sử dụng để phân tích mẫu tổng hợp được là DTA-TGA, XRD, BET, SEM. Vật liệu tổng hợp ở các điều kiện tối ưu được ứng dụng xử lí methylene blue (MB) trong môi trường nước. Kết quả phân tích MB cho thấy hiệu suất xử lí đạt gần 80 % ở pH4, nồng độ đầu vào của chất ô nhiễm 10 ppm, hàm lượng chất xúc tác 1 g/L. 
Từ khóa: CeO2, PVA, tartaric acid, MB
Synthesis of CeO2 and its application for treating organic dyes in water
ABSTRACT
The CeO2 material was synthesized using two gelling agents: tartaric acid (A) and polyvinyl alcohol (P) through the combustion method. DTA-TGA, XRD, BET, and SEM methods were employed to analyze the characteristics of the synthesized material. The synthesized materials, prepared under optimal conditions, were utilized for the treatment of methylene blue (MB) in water. The efficiency achieved nearly 80 % at pH4 with an input concentration of the pollutant at 10 ppm and a catalyst concentration of 1 g/L.
Keywords: CeO2, PVA, tartaric acid, methylene blue.
1. INTRODUCTION 
Currently, environmental pollution poses a significant global challenge, including in Vietnam. Untreated or improperly treated waste released into the environment pollutes the soil, water, and air, directly impacting human life. Various methods are being applied and researched to treat pollutants, each with its own set of advantages and disadvantages.
Recently, photocatalytic method using CeO2 catalyst has received research attention. Research results showed the effectiveness of CeO2 in treating pollutants that are difficult to biodegrade1,2 as well as pigments3,4. The advantages of CeO2 are manifested in its structure. According to research5, in the unit structure of CeO2, the cation Ce4+ was easily replaced by Ce3+. To compensate for the charge, the part of the oxygen elements were lost and created oxygen vacancies. Therefore, CeO2 was converted to the form CeO2-n. These oxygen vacancies were the reason for their effectiveness in catalytic reactions.
CeO2 material was synthesized by many different methods such as hydrothermal6, sol-gel7, combustion method8...or a combination of methods. The combustion method offers the advantage of simplicity and the capability to synthesize a large quantity of material. In this study, two gelling agents, PVA and tartaric acid, were combined. The addition of tartaric acid to the reaction mixture enhanced its complexation ability, provided additional heat, reduced the concentration of PVA, and lowered the synthesis temperature of the material.
2. EXPERIMENT
2.1. Material synthesis process
Oxide nanoparticles of CeO2 were synthesized by the combustion method. The gelling agents were dissolved in water with salt solutions of Ce3+ in appropriate molar ratios. The solution was stirred and heated until transparent gel was formed. The formation gel had high viscosity and was dried for 2 hours at 110 oC. Finally, it formed a puffy, spongy mass. Material products were obtained after calcinating at different temperatures. pH buffers were used to investigate desire pH. The chemicals used in this study were analytical quality.
2.2. Photocatalytic process 
Research investigated the degradation of MB via photocatalytic processes employing CeO2 nanoparticle oxides. Initially, a solution containing a specified concentration of the contaminant and catalyst was introduced into the reactor system (250 mL). Following this, the suspension was stirred in darkness for 60 minutes to establish an adsorption/desorption equilibrium before irradiation. Afterthat, the mixture was lit by LED light with power 220 V, 30 W with different times. At specific time points, approximately 5 mL of the mixture was withdrawn, centrifuged, and subsequently filtered to remove the residual catalyst particulates for analysis. The concentration of MB was determined using UV-Vis spectroscopy (CE-2011) at a wavelength of 663 nm.

Top of Form

3. RESULTS AND DISCUSSION 
3.1. Effect of calcination temperature
Different thermal analysis method was used to investigate calcination temperature of dried sample synthesized gelation temperature of 80 ℃; pH4; Ce/AP ratio = 1/3; AP ratio = 1/1. The results were shown in figure 1.
[image: image1.png]HeatFlow (mW)

TG (mg)

0 100 200 300 400 500 600 700 800 900

Sample Temperature (°C)




Figure 1. DTA – TGA of gel sample 

Figure 1 depicts a rapid weight loss observed within the temperature range of 30 to 300 ℃, attributed to both dehydration and decomposition of PVA and tartaric acid within the sample. This phenomenon aligns with the distinct exothermic peak recorded at 236.09 ℃ on the DTA curve. Subsequently, minimal mass variation was noted above the TGA curve, indicative of the formation of the pure product.

To examine the formation of CeO2 material, the sample underwent calcination at various temperatures. The outcomes are illustrated in Figure 2.

[image: image2.png](0cP) i+

(LEE) Mmp ﬁq |

(00%): :

(¢ze
(LLE) <

e

AONNYInL

i

(002)
(LLL)

(ne) Alsuaju|

30 40 50 60 70 80
2 theta (degree)

20




Figure 2. XRD diagrams of samples at different temperatures a)300 ℃; b)400 ℃; c)450 ℃; d)500 ℃; e)600 ℃; f)700 ℃
The peaks located at 2θ = 28.5; 33.1; 47.5; 56.5; 59.1; 70.0; 76.5 and 79.5 correspond to the (111), (200), (220), (311), (222), (400), (331), and (420) crystal planes of CeO2, respectively, according to JCPDS card: 34-03949. These peaks began to appear at low temperatures of 300 ℃, and the peaks formed more clearly when sample was calcined at higher temperatures. Here the calcination temperature of 400 ℃ was chosen for further studies.
3.2. Effect of pH

After choosing the appropriate calcination temperature, the sample was surveyed to select the optimal pH for the synthesis process. Sample was kept at conditions: gelation temperature 80 ℃; Ce/AP ratio = 1/3; AP ratio = 1/1; calcinating temperature 400 ℃ and pH values were changed by pH2, pH3, pH4. The results were shown in figure 3.
[image: image3.png](ne) Alsuaju|

30 40 50 60 70 80
2 theta (degree)

20




Figure 3. XRD diagrams of samples at a)pH2; b)pH3; c)pH4
Figure 3 distinctly displays the formation of diffraction peaks specific to CeO2. The findings indicate that pH did not significantly influence the phase formation process of CeO2 oxide in this study. However, if the pH is low (pH2, pH3), it can break the polymer chains of PVA, reducing the uniform dispersion of metal cations in the network. The appropriate pH here is pH3, pH4. In the next study, pH 4 was chosen.
3.3. Effect of Ce/AP ratio
The ratio of metal and the gelling agent mixture were studied. The sample was synthesized at a gelation temperature of 80 ℃; AP ratio = 1/1; calcinating temperature 400 ℃; pH4; and Ce/AP ratios were changed at values of 9/1; 3/1; 1/1; 1/3; 1/9. Figure 4 showed the results of XRD diagrams of the synthesized samples.
[image: image4.png]Mﬂv v o

1EE |
(0ov){ |
(2z2)

(LLE) A

(ne) Alsuaju|

30 40 50 60 70 80
2 theta (degree)

20




Figure 4. XRD diagrams of samples with different Ce/AP ratios a)Ce/AP = 9/1; b)Ce/AP = 3/1; c)Ce/AP = 1/1; d)Ce/AP =1/3; e)Ce/AP = 1/9
At ratios of Ce/AP = 9/1; Ce/AP = 3/1; Ce/AP = 1/1 of the amount of agent used to form complexes with metal ions were not enough, resulting gels exhibited poor viscosity. When forming gels at Ce/AP = 1/3 and 1/9, it ensured the appropriate amount of gel-forming agent, leading to high viscosity gels. Upon thermal treatment, the products showed increased porosity and more uniform particle sizes. However, as shown in Figure 4, at the Ce/AP = 1/9, the peaks formed were higher and sharper compared to the Ce/AP = 1/3. This may indicate an increase in the crystal size of the obtained material. Therefore, the Ce/AP = 1/3 was chosen for further studies.
3.4. Effect of gel formation temperature
To investigate gel formation temperature, the sample was synthesized at conditions Ce/AP ratio = 1/3; AP ratio = 1/1; calcinating temperature 400 ℃; pH4, and gel formation temperatures were changed at 40 ℃, 60 ℃, 80 ℃, 100 ℃. The results were shown in Figure 5.

[image: image5.png]80

(0Zv)io 0O e ©
(LEE
(001 { -2
(222) - @
(LLE
(022)
(002)
(LL1) B

(ne) Alsuaju|

2 theta (degree)




Figure 5. XRD diagrams of sample at different gel formation temperatures a)40 ℃, b)60 ℃, c)80 ℃, d) 100 ℃
The synthesis time for sample preparation was observed to be prolonged, taking 8 hours at 40 ℃ and 4 hours at 60 ℃. Surprisingly, at 100 ℃, although the synthesis duration was shorter (an hour), the characteristic peaks of CeO2 were distinctly evident in the XRD pattern. However, significant noise in the background suggested potential instability in the product. Conversely, at 80 ℃, the synthesis duration of 2 hours was sufficient for uniform distribution of metal ions within the complexing agent's network, resulting in clear and well-defined peaks of CeO2 in the XRD pattern. Consequently, a temperature of 80 ℃ was selected for synthesizing the desired sample.
3.5. Material characteristic after choosing optimum conditions
The CeO2 oxide successfully synthesized under the studied conditions was employed for decomposing pollutants via a photocatalytic process. This process was notably influenced by factors such as grain size, material surface area, and more. The material characterization results are presented in Figure 6 and Table 1.
[image: image6.png]



Figure 6. TEM image of CeO2
Figure 6 showed that the oxide nanoparticles of CeO2 were spherical with an average size of about 10 nm. When compared with similar studies10,11 that used only alone gelling agent the results were shown in Table 1.
Table 1. Comparision of CeO2 material formed by using gel agents PVA, AT and mixture of PVA and AT

	Gel agent
	Calcination temperature (℃)
	BET (m2/g)
	TLTK

	PVA
	180
	35.0
	[10]

	AT
	600
	38.57
	[11]

	AP
	400
	72.97
	This study


The calcination temperature of the sample using the AP gelling agent mixture was lower by 200 ℃ compared to the sample using AT alone. Additionally, the specific surface area of the sample using the AP gelling agent mixture was nearly double that of the sample using the gelling agent alone. This demonstrates the advantage of employing a mixture of gelling agents, PVA and AT. The combination enhanced the ability to form complexes with AT and achieve even distribution on the structural net of PVA. The even distribution of heat reduced the required heating temperature, resulting in a final product with a larger specific surface area, thereby creating favorable conditions for the decomposition of pollutants. Figure 7 shows the N2 adsorption–desorption isotherms and the pore size distribution plot of the CeO2 samples.
[image: image7.png]120

12 - p
— 0.10 1 -'- \
1004 £.i 1
— 5 j -
0p) P AV . —— 5
O) § 0.06 \ » /-/
‘E 30 - 80041 '
8 0.02-: /
© 0008 20 40 60 80 100 ‘/"
8 60 _ Pore Width (nm) "‘,"
o e ;
N ‘,0" 4/4
g 4’4/
z 40- « '
-— A~
- P
S 411*“‘
| € —«— Adsorption
0 —eo— Desorption
0.0 0.2 04 0.6 0.8 1.0

Relative Pressure (p/p°)





Figure 7. Nitrogen adsorption–desorption isotherm and the pore size distribution plot for the synthesized CeO2 sample
Figure 7 show that the adsorption and desorption isotherms of the CeO2 material samples exhibit type IV (according to the IUPAC classification), characteristic of mesoporous structures. The average pore diameter was calculated using the BJH method to be 9.7 nm.
3.6. Photocatalytic process to decompose organic pigment of CeO2  material
3.6.1.Effect off catalyst concentration
The material was continued to research on the influence of catalyst content on the MB decomposition process. The initial concentration of the pollutant was 10 ppm, pH 4, the catalyst content was changed at values of 0.25 g/L, 0.5 g/L, 1g/L, 1.5 g/L. The results were shown in figure 8.
The results demonstrated that as the catalyst content increased, the efficiency of MB treatment also increased over time, reaching its peak at a catalyst content of 1.0 g/L after 7 hours of treatment (80%). However, with a further increase in the catalyst content to 1.5 g/L, the efficiency of MB treatment decreased. This could be attributed to the material's black color, which potentially reduced the amount of light reaching the material, thereby affecting the efficiency of the pollutant treatment process.
[image: image8.png]0 60 120 180 240 300 360 420 480
Time (hour)




Figure 8. Effect of catalyst content to MB decomposistion over time
3.6.2. Effect of initial concentration 
The initial pollutant concentration was changed at 5 ppm, 10 ppm, 15 ppm at pH4, catalyst content 1 g/L. The results were shown in figure 9.
[image: image9.png]C/Co

0.0

60 120 180 240 300 360 420 480

Time (hour)




Figure 9. Effect of initial concentration to MB decomposition over time
The initial concentration of the pollutant greatly affected the pollutant treatment process. MB concentration was increased therefore it led to an increase in the amount of pollutants in the reaction mixture. With the same catalytic content and a certain number of active sites, the amount of MB adsorbed on these active sites were greater. Therefore, the number of active sites were not enough to decompose this amount of pollutant. The efficiency of decomposing pollutants decreased.
During photocatalysis, electron/hole pairs are formed under appropriate light conditions. Similar to the study by Le Thi Thanh Tuyen9, under UV light irradiation, these electrons further react with dissolved oxygen to generate superoxide radical anions (O2•−), while h+ in the valence band reacts with adsorbed water and produces more hydroxyl radicals (•OH). These strong oxidizing radicals are reactive species which are mainly responsible for degradation of MB.
4. CONCLUSION
Oxide nanoparticles of CeO2 were successfully synthesized under optimized conditions: calcination temperature at 400 ℃, pH4, Ce/AP = 1/3, AP = 1/1, and gelation temperature at 80 ℃. The resulting nanoparticles exhibited a spherical shape with an average particle size of approximately 10 nm and a surface area of 72.97 m2/g, nearly doubling that achieved when using either the gelling agent PVA (35 m2/g) or AT (38.57 m2/g) individually.

The photocatalytic process utilizing these CeO2 nanoparticles demonstrated an efficiency of 80 % in treating MB under conditions of pH 4, initial MB concentration of 10 ppm, catalyst content at 1 g/L, and a reaction duration of 7 hours.
ACKNOWLEDGMENTS
This research is conducted within the framework of science and technology projects at institutional level of Quy Nhon University under the project code T2023.798.08.
TÀI LIỆU THAM KHẢO
1. M. Aslam, M.T. Qamar, M.Tahir Soomro, Iqbal M.I. Ismail, Numan Salah, Talal Almeelbi, M.A. Gondal, A. Hmeed. The effect of sunlight induced surface defects on the photocatalytic activity of nanosized CeO2 for the degradation of phenol and its derivatives, Applied Catalysis B: Environmental, 2016, 180, 391 – 402.

2. Kaihang Yea , Ya Lib , Hao Yanga , Mingyang Lia, Yongchao Huang, Shanqing Zhang, Hongbing Ji. An ultrathin carbon layer activated CeO2 heterojunction nanorods for photocatalytic degradation of organic pollutants, Applied Catalysis B: Environmental, 2019, 259, 1 – 8.

3. 
Le Huu Trinh, Nguyen Duc Cuong, Do Dang Trung, Nguyen Van Hieu. Synthesis and characterization of hierarchical CeO2 spherical nanoparticles for photocatalytic degradation of methylene blue, VNU Journal of Science: Mathematics – Physics, 2021, 4, 76 – 85.
4. 
Bakkiyaraj, R., Balakrishnan, M.. Physical, optical and photochemical properties of CeO2 nanoparticles synthesized by solution combustion method,  Journal of Advanced Physics, 2017, 6(1), 41-47. 
5.  Nguyen Thi Hong Tram, Nguyen Dinh Minh Tuan. Synthesis of CeO2 catalyst for complete oxidation of toluene and isopropanol, The University of Danang-Journal of Science and Technology, 2021, 19(3), 29-32.
6.
A.I.Y. Tok, F.Y.C. Boey, Z. Dong, X.L. Sun. Hydrothermal synthesis of CeO2 nano-particles, Journal of materials processing technology, 2007, 190, 217-222.
7. 
P. Periyat, F. Laffir, S. A. M. Tofail, E. Magner.  A facile aqueous sol–gel method for high surface area nanocrystalline CeO2, RSC advances, 2011, 1, 1794 – 1798. 
8. 
Mokkelbost, T., Kaus, I., Grande, T., & Einarsrud, M. A.. Combustion synthesis and characterization of nanocrystalline CeO2-based powders, Chemistry of materials, 2004, 16(25), 5489-5494.
9. Le Thi Thanh Tuyen, Dinh Quang Khieu, Hoang Thai Long, Duong Tuan Quang, Chau The Lieu Trang, Tran Thai Hoa and Nguyen Duc Cuong. Monodisperse Uniform CeO2 Nanoparticles: Controlled Synthesis and Photocatalytic Property, Journal of Nanomaterials, 2016, vol. 2016.
10. Nguyen Gia Hung, Luu Minh Dai, Vo Quang Mai, Dao Ngoc Nhiem. Low temperature synthesis of nanostructured cerium dioxide by auto combustion process of polyvinyl alcohol-cerium nitrate gel, Journal of Chemistry, 2004, 42, 444 – 448.
11. Vo Quang Mai, Tran Thi Cuc Phuong. Synthesis of ultrafine CeO2 via sol-gel method from Cerium (IV) nitrate and tartaric acid,  Hue University Journal of Science, 2008, 48,  119 – 124.

1

