Nghiên cứu khả năng hấp phụ và tách lọc carbon dioxide 
của vật liệu MIL-53(Cr) bằng phương pháp mô phỏng cổ điển

Nguyễn Thị Xuân Huynh1,2,*, Trần Thị Diễm Thanh1,2, Nguyễn Lê Bảo Trân1,2, Nguyễn Ngọc Khoa Trường1

1Khoa Khoa học Tự nhiên, Trường Đại học Quy Nhơn, 170 An Dương Vương, Quy Nhơn, Bình Định

2Phòng Hóa tính toán và Mô phỏng, Trường Đại học Quy Nhơn, 170 An Dương Vương, Quy Nhơn, Bình Định

*Tác giả liên hệ chính. Email: nguyenthixuanhuynh@qnu.edu.vn

cm)

TÓM TẮT

Các nguồn năng lượng dựa trên nhiên liệu hóa thạch ngày càng cạn kiệt và lượng khí thải độc hại, đặc biệt là carbon dioxide (CO2), đang tăng rất nhanh và báo động đến môi trường và sức khỏe con người. Do đó, việc làm giảm hoặc chuyển đổi CO2 thành các hợp chất có giá trị là hết sức cấp thiết. Trong những thập niên gần đây, việc ứng dụng các vật liệu có độ xốp cao như nhóm vật liệu khung kim loại hữu cơ (MOF) để hấp phụ CO2 và tách lọc khí CO2/H2 đang rất thu hút. Trong các vật liệu MOF, MIL, đặc biệt là MIL-53 rất được chú ý với khả năng hấp phụ và tách lọc cao nhờ vào tính ổn định nhiệt, diện tích bề mặt riêng lớn và chứa các vị trí kim loại mở, v.v. Do vậy, công trình này muốn làm sáng tỏ khả năng hấp phụ và tách lọc CO2 ở nhiệt độ phòng và áp suất thấp dưới 50 bar bằng phương pháp mô phỏng Monte Carlo chính tắc lớn. Kết quả chỉ ra MIL-53 có khả năng hấp phụ CO2 cao kể cả khi có và không có mặt H2 và độ tách lọc CO2/H2 cũng rất đáng chú ý. Lượng khí CO2 (tinh khiết) hấp phụ trong MIL-53(Cr) đạt được là 9,18 mmol/g ở 298 K và 50 bar. Ở 298 K, độ tách lọc CO2/H2 cực đại của MIL-53(Cr) là SCO2/H2(max)= 116. Kết quả đáng chú ý đó là SCO2/H2(max) gần như không phụ thuộc vào tỉ lệ mol CO2:H2 mà chỉ làm thay đổi áp suất đạt được SCO2/H2(max) đó, nhưng lại phụ thuộc rất mạnh vào nhiệt độ, cụ thể SCO2/H2(max) = 245 khi giảm nhiệt độ đến 273 K.

Từ khóa: Hấp phụ CO2, Bắt giữ CO2, Tách lọc CO2/H2, Vật liệu MIL-53, Mô phỏng cổ điển.

A classical simulation study for carbon dioxide adsorption and separation capacity of MIL-53(Cr)

Nguyen Thi Xuan Huynh1,2,*, Tran Thi Diem Thanh1,2, Nguyen Le Bao Tran1,2, and Nguyen Ngoc Khoa Truong1

1Faculty of Natural Sciences, Quy Nhon University, 170 An Duong Vuong, Quy Nhon, Binh Dinh

2Lab of Computational Chemistry and Modelling, Quy Nhon University, 170 An Duong Vuong, Quy Nhon, Binh Dinh

*Corresponding author. Email: nguyenthixuanhuynh@qnu.edu.vn

cm)

ABSTRACT

In addition to the escalating depletion of fossil fuel-based energy sources, toxic emissions, particularly carbon dioxide (CO2), are rapidly increasing, leading to an alarming impact on the environment and human health. Therefore, reducing or converting CO2 into high-value chemicals is necessary. In recent decades, CO2 capture and CO2/H2 separation based on the adsorption of highly porous materials, especially metal-organic frameworks (MOFs), has become very attractive. Among MOFs, MIL, notably MIL-53, has been a top concern for its noteworthy adsorption and separation capacity due to its thermal stability, ultra-high specific surface, open metal sites, etc. Therefore, this work mainly uses grand canonical Monte Carlo simulations to study CO2 adsorption and separation with and without H2 at room temperatures and low pressures below 50 bar. The high CO2 adsorption capacity with and without hydrogen and remarkable CO2/H2 selectivity of MIL-53(Cr) are explored. For pure CO2, the absolute CO2 uptake in MIL-53(Cr) is 9.18 mmol/g at 298 K and 50 bar. Besides, the maximum CO2/H2 selectivity of MIL-53(Cr) is SCO2/H2(max)= 116 at 298 K. Remarkably, this value of SCO2/H2(max) is almost independent on the CO2/H2 mole fraction, which only changes pressure corresponding to that SCO2/H2(max), but dramatically dependent on temperature, reaching SCO2/H2(max)= 245 when the temperature drops to 273 K.

Keywords: CO2 adsorption, CO2 capture, CO2/H2 selectivity, MIL-53 material, classical simulations.

1. INTRODUCTION

Fossil fuels are our primary energy source, and their consumption is increasingly uncontrollable. This problem has a significantly negative impact on the environment and human health due to the increasing amount of emissions such as CO2, CO, NOx, etc., and causes serious energy shortage issues. Furthermore, CO2 capture, H2 purification, and CO2 separation over H2 are significant in combustion plants and refineries.1–3 To overcome those problems, the demand for clean energy production, gas separation, and efficient storage has been growing dramatically. Tremendous advances have been achieved in both theory and experiments thanks to the outstanding properties of porous materials.4–6

A new type of inorganic-organic hybrid porous materials, metal-organic frameworks (MOFs) with a periodic network, appears as a potential technology.6–9 Since the early 1990s, MOFs have gained increasing attention, leading to more MOFs have been successfully synthesized by experiments and proposed by simulation methods. Researchers have successfully synthesized about 100,000 MOFs through experiments and have predicted over 500,000 structures by simulations or theories, but only nearly 3,500 works related to MOFs have been published.10,11

MILs (Material Institute of Lavoisiers), a class of MOFs,  have gained recognition as promising adsorbents for H2 purification and CO2 capture thanks to unique properties such as extraordinary chemical and thermal properties, water stability, ultra-large specific surface areas, high porosity, coordinately unsaturated or open metal sites, etc.12–15 In 2002, the first MIL introduced by Ferey and co-workers was the MIL-53 with M = chromium(III) (Cr3+).16,17 MIL-53,  obtained by the hydrothermal method, has many potential applications because of its good thermal stability and flexibility compared to other MOFs.18,19 Several works have displayed that MIL-53 (Cr or Al) materials have superior CO2 capture20–22 and high selective adsorption for binary mixtures such as CO2/H2, CO2/CH4, and CO2/N2.19,23,24

Due to the potential of MIL-53, in this work, we use the classical grand canonical Monte Carlo (GCMC) simulation (a suitable approach to simulate the equilibrium of the physisorption of small gases in porous at well-defined pressure and temperature) to study the capacities of CO2 capture and CO2/H2 separation on MIL-53(Cr).

2. COMPUTATIONAL APPROACHES

GCMC simulations are carried out using the RASPA software25 to calculate the gravimetric amount of gases (CO2 and H2) adsorbed in a solid porous material, MIL-53(Cr), at room temperature and pressures up to 50 bar. The simulation cycles are performed up to 3.0 ×105 Monte Carlo (MC) cycles followed by 1.5×104 equilibration steps.

In order to obtain the simulation box, a unit cell of MIL-53 (including 20 hydrogen, 32 carbon, 20 oxygen, and 4 chromium) was optimized by using the density functional theory (DFT),26 and then repeated the unit cell to 2, 2, and 4 times for a, b, and c lengths (Å,  Å, Å), leading to  Å,  Å, and  Å, respectively (Figure 1).

Figure 1. The simulation box of MIL-53(Cr). Each rectangular cubic represents a unit cell.

The interactions between gases (CO2, H2) and MIL-53(Cr) include (i) van der Waals (vdW) interactions using the Lennard-Jones (LJ) model and (ii) electrostatic interactions.

First, the LJ 12-6 repulsive and attractive interactions between pairs of atoms of gases and MIL-53 are described by

,	(1)

Herein, εij and σij are pair LJ parameters, calculated using the pair combining rule of Lorentz and Berthelot,25 in which σi and εi are taken from the force fields for MOFs with universal force field for metal (Cr) and DREIDING for other elements of MIL-53 (H, C, O),27 listed in Table 1. The cut-off radius used for the vdW interaction is 16 Å, tested for reliability.

Second, electrostatic or Coulomb interactions between pairs of atoms are as follows:

,	(2)

where kc is the Coulomb constant and qi is the partial point charge of atom i, calculated by the DFT-based density-derived electrostatic and chemical charges (Table 1 with the labeled atoms as in Figure 2).28 Additionally, TraPPE force fields are used for CO2 and H2, listed in Table 1.

The adsorption separation or selectivity of CO2 over H2 in a mixture of H2 and CO2 is calculated via the formula13

,	(3)

where are the amount of adsorbed CO2 and H2 (mol/g) in MIL-53 and are mole fraction of the CO2 and H2 component in the mixture, respectively. The investigated molar fractions of CO2:H2 includes 1:9, 2:8, 3:7, 4:6, 5:5, 6:4, 7:3, 8:2, 9:1.

Figure 2. The labeled atoms of MIL-53(Cr), where hydrogen (H), carbon (C), oxygen (O), and chromium  (Cr) atoms are displayed by soft pink, brown, red, and blue balls, successively.

Table 1. LJ parameters and partial atomic charges of MIL-53 and gases (H2 and CO2).

| Atoms | /kB (K) | (nm) | Atomic charges (e) |
| --- | --- | --- | --- |
| Cr | 7.548 | 0.269 | +1.581 |
| H1 | 7.649 | 0.285 | +0.414 |
| H2 |  |  | +0.100 |
| C1 | 47.856 | 0.347 | -0.077 |
| C2 |  |  | +0.636 |
| C3 |  |  | -0.033 |
| O1 | 48.158 | 0.303 | -0.589 |
| O2 |  |  | -0.938 |
| C [CO2]29 | 27.000 | 0.280 | +0.700 |
| O [CO2]29 | 79.000 | 0.305 | -0.350 |
| HCOM [H2]30 | 36.700 | 0.296 | -0.936 |
| H [H2]30 | - | - | +0.468 |

3. RESULTS AND DISCUSSION

3.1. CO2 adsorption of MIL-53(Cr)

Firstly, the absolute CO2 adsorption capacity or uptake is computed and compared with available experimental data. The results (Figure 3) show that the CO2 uptake increases rapidly in the pressure region below 5 bar, then increases slightly with increasing pressure. The absolute CO2 uptake is 9.18  0.02 mmol/g or ​​403.70  0.88 mg/g at 50 bar (the maximum excess CO2 uptake is 8.02  0.02 mmol/g or 387.23  0.93 mg/g at 30 bar). Our findings show that the absolute amount of CO2 adsorption on MIL-53(Cr) is consistent with the available data of Bourrelly et al., about 10 mmol/g at 30 bar and 304 K.20 Otherwise, the obtained CO2 adsorption heat of MIL-53(Cr) is 30.04 kJ/mol, consistent with data of Bourrelly and co-workers (about 32 kJ/mol).20 We also find that, at 298 K, the CO2 adsorption isotherm obtained from molecular simulations also agrees well with the experimental results of the Schneemann group (Figure 3).31 These agreements between simulation and experimental measures indicate the reliability of the GCMC simulations.

Figure 3. The comparison of the absolute CO2 adsorption capacity on MIL-53(Cr) at 298 K between GCMC simulation and experimental (expt.) data.31

MIL-53(Cr) does not capture CO2 as strongly as the most highly evaluated MOFs available today; however, these results are comparable to the MIL-88 series (4.0 – 12.1 mmol/g), highly evaluated for CO2 uptakes14 with the isosteric heat of adsorption of the MIL-88 series (31.8 – 34.9 kJ/mol).

Next, we study the co-adsorption capacity of MIL-53 for H2 and CO2 in their mixture at many different mole fractions (CO2:H2 = 1:9, 2:8, 3:7, 4:6, 5:5, 6:4, 7:3, 8:2, 9:1) at 298 K and pressures p ≤ 50 bar. Our simulations also exhibit that the CO2 adsorption is much higher than H2 because of its high isosteric heat of adsorption (30.04 kJ/mol) compared to H2 (12.87 kJ/mol) at 298 K and in the low-pressure range. Indeed, Figure 4 shows that MIL-53(Cr) adsorbs CO2 (9.16 → 6.26 mmol/g) superiorly than H2 (0.02 → 0.55 mmol/g) when the molar ratio of CO2:H2 changes from 1:9 to 9:1. Indeed, the CO2 uptake insignificantly decreases when the molar ratio of H2 increases, less than 70% in the mixture, i.e. decreasing from 9.18 mol/g (pure CO2) to 8.37 mmol/g with 8.82% at CO2:H2 = 4:6. When the mole fraction of H2 occupies a large portion of the mixture, the CO2 uptake decreases significantly. More specifically, the CO2 uptake in MIL-53(Cr) decreases by 12.64% (9.18 → 8.02 mmol/g), 18.52% (9.18 → 7.48 mmol/g), and 31.81% (9.18 → 6.26 mmol/g) when the molar ratio of H2 is 70% (CO2:H2 = 3:7), 80% (CO2:H2 = 2:8), and 90% (CO2:H2 = 1:9) compared with pure CO2 uptake (Table 2). These data demonstrate that MIL-53(Cr) has good selective adsorption of separation for CO2 over H2 in the binary mixture of CO2 and H2.

Table 2. The absolute CO2 and H2 uptakes of MIL-53(Cr) with the different mole fractions of CO2:H2, compared to pure CO2 uptake at room temperature.

| CO2:H2 mole- fraction | CO2 uptake (50 bar) | Decrease in comparison to pure CO2 (%) | H2 uptake (50 bar) |
| --- | --- | --- | --- |
| Pure CO2 | 9.18 |  | - |
|  | 10 (30 bar)20 |  | - |
| 9:1 | 9.16 | 0.22 | 0.02 |
| 8:2 | 9.08 | 1.09 | 0.04 |
| 7:3 | 8.95 | 2.51 | 0.06 |
| 6:4 | 8.80 | 4.14 | 0.09 |
| 5:5 | 8.61 | 6.21 | 0.12 |
| 4:6 | 8.37 | 8.82 | 0.16 |
| 3:7 | 8.02 | 12.64 | 0.22 |
| 2:8 | 7.48 | 18.52 | 0.32 |
| 1:9 | 6.26 | 31.81 | 0.55 |

Figure 4. The CO2 and H2 co-adsorption isotherms of MIL-53(Cr) at 298 K with different CO2:H2 ratios from 1:9 to 9:1. Solid and dot lines refer to the adsorption amount of CO2 and H2 on MIL-53(Cr). The black dashed line represents pure CO2 adsorption on MIL-53(Cr).

3.2. CO2/H2 separation of MIL-53(Cr)

From Figure 5b, it can be seen that, at 298 K, the highest selectivity achieved for each CO2:H2 mole-fraction greatly depends on pressure. Specifically, they sharply increase at low pressure, reach a peak with the maximum selectivity of CO2/H2, and then gradually decrease with pressure to 50 bar. As a result, the maximum CO2/H2 selectivity is different for mole ratios of the gas mixture, listed in Column 3 of Table 3 (298 K). When the CO2 mole-fraction increases, the selectivity reaches its maximum at low pressure 
(5 – 25 bar). More detail, the maximum selectivity SCO2H2(max)= 107.87 at 25 bar for CO2:H2 = 1:9, …, and SCO2H2(max)=118.25 at 5 bar for CO2:H2 = 9:1 (Table 3). Nevertheless, the maximum selectivity does almost not change with the change of the mole ratio between CO2 and H2, SCO2/H2= 116 (pink line in Figure 6). This trend is similar to the case of MOF5 and Cu-BTC studied previously.32,33 Remarkably, our data also shows that the CO2/H2 selectivity, SCO2H2 of MIL-53(Cr) is higher to that of many previous MOFs such as microporous silica (3.5), activated carbon (45.0), zeolites Na-4A (70.7), Cu-BTC (SCO2H2(max)≈  150 at 12.5 bar), MOF-5 (SCO2H2(max)≈  36 at 50 bar)32 and IR-MOF-n with n=9, 10,⋯,14 (SCO2H2(max)≤  100).33

Furthermore, in this study, we also clarify the effect of temperature on the selectivity of CO2/H2 in MIL-53(Cr). Therefore, we performed further research at temperatures of 273 K, 323 K, and 348 K surrounding 298 K. The obtained results, visualized in Figure 5, indicate that the selectivity sharply increases as the temperature decreases. Besides, the pressure at which SCO2/H2 is maximal decreases with the lowering temperature (Figure 5 and Table 3).  For instance, with CO2:H2 = 5:5, the maximum selectivities are SCO2H2(max)= 39.81 at 15 bar (348 K), 65.17 at 10 bar (323 K), 118.31 at 7.5 bar (298 K), and 246.43 at 2.5 bar (273 K).  Figure 5 also shows that the peaks representing the maximum CO2/H2 selectivity also reduce as the temperature increases.  The maximum CO2/H2 selectivity and the pressure corresponding to different mole ratios at four temperatures are listed in Table 3.

Surprisingly, the obtained maximum SCO2/H2 values are nearly constant when the CO2 mole-fraction changes from 1/10 to 9/10 of the binary mixture. We determine the average maximum selectivities, SCO2/H2 = 245, 116, 64, and 39 at 273 K, 298 K, 323 K, and 348 K, respectively (Figure 6). This work also shows that the CO2/H2 separation significantly increases with decreasing temperature. More importantly, for the maximum SCO2/H2, when the temperature drops from 348 K to 273 K, the variation of CO2/H2 separation dramatically increases with ∆SCO2/H2= 25 (348 K to 323 K), 53 (323 K to 
298 K), 128 (298 K to 273 K). Therefore, in order to effectively increase the CO2 selective adsorption in the mixture (CO2 and H2), the temperature can be reduced to achieve the desired separation at suitable pressures for the determined CO2/H2 mole-fraction.

Table 3. Maximum CO2/H2 selectivity versus mole ratios of CO2/H2 at 273 K, 298 K, 323 K, and 348 K.

| CO2:H2 | 273 K | 298 K | 323 K | 348 K |
| --- | --- | --- | --- | --- |
| 1:9 | 233.97 (15 bar) | 107.87 (25 bar) | 57.73 (40 bar) | 35.27 (50 bar) |
| 2:8 | 243.04 (7.5 bar) | 114.30 (15 bar) | 61.95 (30 bar) | 37.82 (30 bar) |
| 3:7 | 244.17 (5 bar ) | 116.68 (10 bar) | 63.55 (20 bar) | 38.75 (20 bar) |
| 4:6 | 246.44 (5 bar) | 117.30 (7.5 bar) | 64.33 (15 bar) | 39.54 (20 bar) |
| 5:5 | 246.43 (2.5 bar) | 118.31 (7.5 bar) | 64.74 (10 bar) | 39.81 (15 bar) |
| 6:4 | 248.46 (2.5 bar) | 118.34 (5 bar) | 65.17 (10 bar) | 39.95 (15 bar) |
| 7:3 | 248.44 (2.5 bar) | 118.96 (5 bar) | 64.89 (7.5 bar) | 40.02 (10 bar) |
| 8:2 | 247.38 (2.5 bar) | 116.78 (5 bar) | 65.23 (7.5 bar) | 40.04 (10 bar) |
| 9:1 | 243.44 (2.5 bar) | 118.25 (5 bar) | 65.37 (5 bar) | 40.02 (7.5 bar) |

Figure 5. CO2/H2 selectivity of MIL-53(Cr) with different CO2/H2 mole fractions  at temperatures: (a) 273 K, (b) 298 K, (c) 323 K, and (d) 348 K.

Figure 6. Dependence of maximum CO2/H2 selectivity on the mole ratios of CO2 at 273 K, 298 K, 323 K, and 348 K. The values ​​in parentheses refer to the pressure at which the CO2/H2 selectivity is maximum.

4. CONCLUSIONS

This study obtained the important results as follows:

-	The CO2 uptakes in MIL-53(Cr) are high even with the H2 absence and presence. The CO2 capture capacity insignificantly decreases when the molar fraction of H2 increases no more than 60%, i.e., decreasing from 9.18 mmol/g (pure CO2) to 8.37 mmol/g (CO2:H2 = 4:6) with 8.82%.

-	The high CO2/H2 selectivity is also elucidated at various molar fractions of CO2:H2 and at different temperatures (273 K, 298 K, 323 K, and 348 K). The results exhibit that when the CO2 mole-fraction in the binary mixture increases, the maximum CO2/H2 selectivity remains nearly constant, but the pressure corresponding to this maximal selective adsorption remarkably decreases. Moreover, the temperature strongly affects the CO2 over H2 separation capacity (116 to 245 for maximum CO2/H2 selectivity with decreasing temperature 298 K to 273 K). This work evidences that reducing the temperature can increase the selective adsorption efficiency of CO2/H2. Additionally, adjusting the mole fraction between hydrogen and carbon dioxide can help achieve the CO2/H2 selectivity at low pressure.

Acknowledgments

This study is conducted within the framework of science and technology projects at the institutional level of Quy Nhon University under project code T2023.794.04. We also acknowledge support for the calculations from the Lab of Computational Chemistry and Modeling (LCCM), Quy Nhon University, Vietnam.

References

1.	G. Avci, I. Erucar and S. Keskin. Do new mofs perform better for CO2 capture and H2 purification? Computational screening of the updated mof database, ACS Appl. Mater. Interfaces, 2020, 12, 41567–41579.

2.	H. Demir, G. O. Aksu, H. C. Gulbalkan and S. Keskin. MOF membranes for CO2 capture: Past, present and future, Carbon Capture Sci. Technol., 2022, 2, 100026.

3.	B. Dziejarski, J. Serafin, K. Andersson and R. Krzyżyńska. CO2 capture materials: A review of current trends and future challenges, Mater. Today Sustain., 2023, 24, 100483.

4.	L. F. Chuah, A. Bokhari, S. Asif, J. J. Klemeš, D. J. Dailin, H. El Enshasy and A. H. M. Yusof. A review of performance and emission characteristic of engine diesel fuelled by biodiesel, Chem. Eng. Trans., 2022, 94, 1099–1104.

5.	X. Tan, S. Wang and N. Han. Metal organic frameworks derived functional materials for energy and environment related sustainable applications, Chemosphere, 2023, 313, 137330.

6.	Y. Cao, X. Li, G. Yu and B. Wang. Regulating defective sites for pharmaceuticals selective removal: Structure-dependent adsorption over continuously tunable pores, J. Hazard. Mater., 2023, 442, 130025.

7.	G. Ferey. Hybrid porous solids: Past, present, future, Angew. Chemie Int. Ed., 2008, 37, 191–214.

8.	H. Furukawa, K. E. Cordova, M. O. Keeffe and O. M. Yaghi. The chemistry and applications of metal-organic frameworks, Science, 2013, 341, 1230444.

9.	I. Hussain, S. Iqbal, C. Lamiel, A. Alfantazi and K. Zhang. Recent advances in oriented metal–organic frameworks for supercapacitive energy storage, J. Mater. Chem. A, 2022, 10, 4475–4488.

10.	S. M. Moosavi, A. Nandy, K. M. Jablonka, D. Ongari, J. P. Janet, P. G. Boyd, Y. Lee, B. Smit and H. J. Kulik. Understanding the diversity of the metal-organic framework ecosystem, Nat. Commun., 2020, 11, 1–10.

11.	H. Daglar and S. Keskin. Recent advances, opportunities, and challenges in high-throughput computational screening of MOFs for gas separations, Coord. Chem. Rev., 2020, 422, 213470.

12.	B. E. Keshta, H. Yu and L. Wang. MIL series-based MOFs as effective adsorbents for removing hazardous organic pollutants from water, Sep. Purif. Technol., 2023, 322, 124301.

13.	D. N. Son, N. Thi, X. Huynh, N. Thoai and P. T. Kien. Highly selective separation of CO2 and H2 by MIL-88A metal organic framework, VNU J. Sci. Math. – Phys., 2021, 37, 9–21.

14.	N. T. X. Huynh, O. K. Le, T. P. Dung, V. Chihaia and D. N. Son. Theoretical investigation of CO2 capture in the MIL-88 series: Effects of organic linker modification, RSC Adv., 2023, 13, 15606–15615.

15.	N. T. X. Huynh, V. Chihaia and D. N. Son. Hydrogen storage in MIL-88 series, J. Mater. Sci., 2019, 54, 3994–4010.

16.	S. Tomar and V. K. Singh. Review on synthesis and application of MIL-53, Mater. Today Proc., 2021, 43, 3291–3296.

17.	C. Serre, F. Millange, C. Thouvenot, M. Noguès, G. Marsolier, D. Louër and G. Férey. Very large breathing effect in the first nanoporous Chromium(III)-based solids: MIL-53 or CrIII(OH)·{O2C−C6H4−CO2}·{HO2C−C6H4−CO2H}x·H2Oy, J. Am. Chem. Soc., 2002, 124, 13519–13526.

18.	F. Millange and R. I. Walton. MIL-53 and its isoreticular analogues: A review of the chemistry and structure of a prototypical flexible metal-organic framework, Isr. J. Chem., 2018, 58, 1019–1035.

19.	F. Millange, C. Serre and G. Férey. Synthesis, structure determination and properties of MIL-53as and MIL-53ht: the first CrIII hybrid inorganic–organic microporous solids, Chem. Commun., 2002, 8, 822–823.

20.	S. Bourrelly, P. L. Llewellyn, C. Serre, F. Millange, T. Loiseau and G. Férey. Different adsorption behaviors of methane and carbon dioxide in the isotypic nanoporous metal terephthalates MIL-53 and MIL-47, J. Am. Chem. Soc., 2005, 127, 13519–13521.

21.	D. Panda, S. Patra, M. K. Awasthi and S. K. Singh. Lab cooked mof for CO2 capture: A sustainable solution to waste management, J. Chem. Educ., 2020, 97, 1101–1108.

22.	J. L. de Miranda, T. P. de Abreu, J. M. B. Neto, D. de Pontes Souza, I. Coelho, F. Stavale, S. de S. A. Oliveira and L. C. de Moura. A case study for an eco-design of aluminum terephthalate metal-organic framework- MIL-53(Al) for CO2 and methane adsorption, Sustain. Mater. Technol., 2023, 37, e00689.

23.	Y. Jiao, Z. Li, Y. Ma, G. Zhou, S. Wang and G. Lu. The studies on gas adsorption properties of MIL-53 series MOFs materials, AIP Adv., 2017, 7, 085009.

24.	P. Rallapalli, K. P. Prasanth, D. Patil, R. S. Somani, R. V. Jasra and H. C. Bajaj. Sorption studies of CO2, CH4, N2, CO, O2 and Ar on nanoporous aluminum terephthalate [MIL-53(Al)], J. Porous Mater., 2011, 18, 205–210.

25.	D. Dubbeldama, S. Calerob, D. E. Ellisc, R. Q. Snurr, D. Dubbeldam, S. Calero, D. E. Ellis and R. Q. Snurr. RASPA: molecular simulation software for adsorption and diffusion in flexible nanoporous materials, Mol. Simul., 2016, 42, 81–101.

26.	J. P. Perdew, K. Burke and M. Ernzerhof. Generalized gradient approximation made simple, Phys. Rev. Lett., 1996, 77, 3865–3868.

27.	A. K. Rappe, C. J. Casewit, K. S. Colwell, W. A. Goddard III and W. M. Skiff. UFF, a full periodic table force field for molecular mechanics and molecular dynamics simulations, J. Am. Chem. Soc., 1992, 114, 10024–10035.

28.	N. Q. Vinh, N. T. M. Duyen, N. L. B. Tran, N. Van Nghia, L. T. T. V. Vien, H. T. M. Thanh and N. T. X. Huynh. Computational study on enhancing SO2 capture capacity of M2(BDC)2TED (M = Mg, V, Co, or Ni), Quy Nhon Univ. J. Sci., 2024, 18, 91–100.

29.	J. J. Potoff and J. I. Siepmann. Vapor-liquid equilibria of mixtures containing alkanes, carbon dioxide, and nitrogen, AIChE J., 2001, 47, 1676–1682.

30.	D. Levesque, A. Gicquel, F. L. Darkrim and S. B. Kayiran. Monte Carlo simulations of hydrogen storage in carbon nanotubes, J. Phys. Condens. Matter, 2002, 14, 9285–9293.

31.	A. Schneemann, V. Bon, I. Schwedler, I. Senkovska, S. Kaskel and R. A. Fischer. Flexible metal-organic frameworks, Chem. Soc. Rev., 2014, 43, 6062–6096.

32.	Q. Yang and C. Zhong. Molecular simulation of carbon dioxide/methane/hydrogen mixture adsorption in metal-organic frameworks, J. Phys. Chem. B, 2006, 110, 17776–17783.

33.	Y. Qingyuan, X. U. Qing, L. I. U. Bei and Z. Chongli. Molecular simulation of CO2/H2 mixture separation in metal-organic frameworks : Effect of catenation and electrostatic interactions, Chinese J. Chem. Eng., 2009, 17, 781–790.

Liên hệ: Nguyễn Thị Xuân Huynh

Trường Đại học Quy Nhơn

170 An Dương Vương, TP. Quy Nhơn, tỉnh Bình Định, Việt Nam

Email: nguyenthixuanhuynh@qnu.edu.vn

Điện thoại: 0989225650