Supplementary

Figure S1. The current change in electrolyte solution

Table S1. Change of temperature into electrolyte solution in electrochemical exfoliated process (supplementary)

| Time Voltage | 0 min | 30 mins | 60 mins | 90 mins | 120 mins |
| --- | --- | --- | --- | --- | --- |
| 4.5 V | 260C | 300C | 320C | 330C | 330C |
| 6 V | 250C | 280C | 300C | 320C | 340C |
| 8 V | 260C | 330C | 350C | 390C | 420C |
| 10 V | 270C | 430C | 510C | 540C | 550C |

Table S2. The current change in electrolyte solution

| Time (min.) | 4.5 V | 6 V | 8 V | 10 V |
| --- | --- | --- | --- | --- |
| 0 | 0.60 | 1.10 | 1.90 | 2.80 |
| 10 | 0.60 | 1.11 | 1.92 | 2.87 |
| 20 | 0.61 | 1.12 | 1.98 | 3.05 |
| 30 | 0.62 | 1.14 | 2.07 | 3.11 |
| 40 | 0.62 | 1.14 | 2.19 | 3.01 |
| 50 | 0.64 | 1.15 | 2.29 | 2.94 |
| 60 | 0.67 | 1.17 | 2.36 | 2.90 |
| 70 | 0.69 | 1.20 | 2.22 | 2.86 |
| 80 | 0.72 | 1.26 | 2.19 | 2.85 |
| 90 | 0.77 | 1.24 | 2.19 | 2.84 |
| 100 | 0.70 | 1.23 | 2.25 | 2.78 |
| 110 | 0.65 | 1.20 | 2.20 | 2.67 |
| 120 | 0.64 | 1.14 | 2.16 | 2.70 |

Table S3. Functional groups on graphene

| Functional groups | Wave number (cm-1) |
| --- | --- |
| C = C | 1632 |
| – OH | 3438 |
| C – O | 1102 |
| COO – H | 1409 |
| C – H | 2926 |

Table S4. The characteristics peaks D, G, 2D of graphite and graphene

| Materials | D (cm-1) | G (cm-1) | 2D (cm-1) |
| --- | --- | --- | --- |
| GP | 1345 | 1578 | 2703 |
| GR-6 | 1337 | 1586 | 2680 |
| GR-8 | 1339 | 1589 | 2657 |
| GR-10 | 1339 | 1584 | 2671 |