Tổng hợp xanh hạt nano ZnO sử dụng dịch chiết lá trầu không và ứng dụng trong pin mặt trời nhạy quang
Đặng Nguyễn Nhật Huy1,  Văn Phạm Đan Thủy1, Nguyễn Việt Nhẩn Hòa1, Yoshiyuki Murata2, Đoàn Văn Hồng Thiện1*
1Khoa kỹ thuật hóa học, Trường Đại học Cần Thơ – Đường 3/2, Ninh Kiều, Cần Thơ, Việt Nam
2sau đại học khoa học môi trường và đời sống, Đại học Okayama, Okayama, 700-8530, Nhật Bản
*Tác giả liên hệ chính. Email: dvhthien@ctu.edu.vn
TÓM TẮT
Nghiên cứu này báo cáo về phương pháp tổng hợp xanh hạt nano ZnO sử dụng dịch chiết từ lá trầu không (Piper betle) làm tác nhân khử và ổn định tự nhiên. Các hạt nano ZnO tổng hợp được đặc trưng bằng các phương pháp XRD, SEM, TEM và quang phổ UV-Vis, xác nhận cấu trúc tinh thể, hình thái cầu và có vùng cấm quang học là 3,26 eV. Sau đó, các hạt nano ZnO được ứng dụng làm điện cực quang anode trong pin mặt trời nhạy quang (DSSC) sử dụng phẩm nhuộm tự nhiên chiết xuất từ vỏ măng cụt. Phân tích hiệu suất quang điện cho thấy DSSC với điện cực đối Pt có hiệu suất cao hơn đáng kể (0,064%) so với điện cực nền carbon (0,007%), chứng minh hoạt tính xúc tác vượt trội của Pt trong việc cải thiện quá trình vận chuyển điện tích. Những kết quả này nhấn mạnh tiềm năng của hạt nano ZnO tổng hợp bằng phương pháp xanh trong các ứng dụng năng lượng bền vững.
Từ khóa: Tổng hợp xanh, hạt nano ZnO, pin mặt trời nhạy quang
Green Synthesis of ZnO Nanoparticles Using Betel Leaf Extract and Their Application in Dye-Sensitized Solar Cells
Dang Nguyen Nhat Huy1,  Dan-Thuy Van-Pham1, Nguyen Viet Nhan Hoa1, Yoshiyuki Murata2, Doan Van Hong Thien1*
1Faculty of Chemical Engineering, Can Tho University – 3/2 Street, Ninh Kieu District, Can Tho City, Vietnam

2Graduate School of Environmental and Life Science, Okayama University, Okayama, 700-8530, Japan
*Corresponding author. Email: dvhthien@ctu.edu.vn
ABSTRACT
This study reports the green synthesis of ZnO nanoparticles using betel leaf (Piper betle) extract as a natural reducing and stabilizing agent. The synthesized ZnO nanoparticles were characterized by XRD, SEM, TEM, and UV-Vis spectroscopy, confirming their crystalline structure, spherical morphology, and an optical bandgap of 3.26 eV. The ZnO nanoparticles were then employed as the photoanode in dye-sensitized solar cells (DSSCs) using a natural dye extracted from mangosteen peel. Photovoltaic performance analysis revealed that DSSCs with a platinum (Pt) counter electrode exhibited a significantly higher efficiency (0.064%) compared to those using a carbon-based electrode (0.007%), demonstrating the superior catalytic activity of Pt in enhancing charge transport. These findings highlight the potential of ZnO nanoparticles synthesized via green methods for sustainable energy applications.
Keywords: Green Synthesis, ZnO nanoparticles, Dye-Sensitized Solar Cells.
1. INTRODUCTION
Over the past decades, fossil fuels have served as the primary energy source for both industrial and domestic applications. However, due to their non-renewable nature, these resources are gradually depleting, posing significant challenges to sustainable development. Projections indicate that the global economy is expected to triple by 2050, leading to a substantial increase in energy demand.
 ADDIN EN.CITE 
1-4
 In this context, solar energy has emerged as a promising alternative due to its sustainability, abundant availability, and minimal environmental impact. Unlike fossil fuel-based energy sources, solar energy does not generate CO2 emissions and is virtually inexhaustible.5
The growing interest in renewable energy has accelerated advancements in solar energy conversion technologies, with dye-sensitized solar cells (DSSCs) receiving considerable attention. DSSCs, which utilize advanced organic materials, represent a significant breakthrough in optimizing solar energy harvesting for electricity generation. These cells offer notable advantages, including a simple fabrication process, low production cost, and efficient operation under diffuse or low-light conditions.
 ADDIN EN.CITE 
5-8
 As a result, DSSCs hold great potential in reducing reliance on fossil fuels and enhancing national energy independence. Additionally, the integration of natural materials in DSSCs, particularly plant-derived dyes and bio-extracted substrates, introduces an environmentally friendly approach to photovoltaic technology.
 ADDIN EN.CITE 
4,8

Zinc oxide (ZnO) is a semiconductor with extensive applications due to its optical transparency, strong luminescence, and high photocatalytic efficiency. In its pure state, ZnO acts as an insulator at low temperatures.
 ADDIN EN.CITE 
3,5,9,10
 However, when heated to approximately 200 – 400 °C, exciton excitation enables ZnO to function as a viable conductive material. Despite its potential, the photocatalytic activity of ZnO remains lower than that of TiO2, necessitating material modifications to enhance its performance.
 ADDIN EN.CITE 
10-12
 In recent years, the green synthesis of ZnO nanoparticles has garnered significant interest due to its reduced consumption of hazardous chemicals, cost-effectiveness, and environmentally benign process. Notably, plant and fruit extracts have been explored as both reaction precursors and stabilizing agents for nanoparticle synthesis.
 ADDIN EN.CITE 
13-18
 The use of eco-friendly solvents, such as water and bio-extracts, facilitates the development of nanostructured materials while eliminating the need for toxic reagents.
 ADDIN EN.CITE 
3,9,11,19-22

Piper betle (commonly known as betel leaf) is a climbing plant belonging to the Piperaceae family, widely cultivated across Asian countries, including Vietnam, India, Thailand, and Indonesia.
 ADDIN EN.CITE 
23-26
 The polyphenolic compounds present in betel leaves serve as both reducing and stabilizing agents in nanoparticle synthesis, effectively controlling morphology and enhancing material stability. According to Raveendran et al., biosynthetic approaches enable the production of nanoparticles with superior structural uniformity and morphological control compared to conventional physicochemical methods.
 ADDIN EN.CITE 
24,26
 In this study, ZnO nanoparticles were synthesized using betel leaf extract as a precursor. Natural dye-sensitized solar cells were subsequently fabricated using ZnO-based nanostructures as the photoanode material. This research not only explores the feasibility of employing cost-effective ZnO as a TiO2 alternative in DSSCs but also contributes to sustainable development by minimizing environmental impact and expanding the applicability of renewable energy technologies.

2. MATERIALS AND METHODS
2.1. Chemicals
Zinc nitrate hexahydrate, potassium hydroxide, ethanol, deionized (DI) water, iodine, ethylene glycol, and potassium iodite were purchased from Merck. Triton X-100 was obtained from Biobasic (Canada), while polyethylene glycol was sourced from Sigma. All chemicals were used as received without further purification.
2.2. Synthesis and characterization methods of ZnO nanoparticles
2.2.1. Green synthesis of ZnO nanoparticles
Betel leaves (Piper betle) were collected from a local source in Can Tho, Vietnam. The leaves were thoroughly washed, cut into small pieces, and subsequently used for extract preparation. A total of 25 g of betel leaves was immersed in 100 mL of distilled water and boiled at 80 °C for 2 hours. After cooling to room temperature, the mixture was filtered to remove solid residues, and the obtained extract was stored at 4 °C for further experiments.

ZnO nanoparticles were synthesized using a green synthesis approach. Specifically, 0.1188 g of zinc nitrate hexahydrate (Zn(NO3)2·6H2O) was dissolved in 100 mL of betel leaf extract under stirring for 10 minutes. The solution was then continuously stirred at 300 rpm at room temperature for 2 hours. Following the reaction, the resulting suspension was centrifuged at 6000 rpm for 15 minutes to separate the solid phase. The obtained solid was dried at 60 °C for 24 hours and subsequently calcined at 500 °C for 30 minutes to obtain ZnO nanoparticles.

2.2.2 ZnO characteristics

X-ray diffraction (XRD, D2 Bruker, Germany) was performed with a scanning angle (2θ) ranging from 20° to 80° at a scanning speed of 0.05°/min to determine the crystal structure, phase composition, and average crystalline size of ZnO nanoparticles.

Scanning electron microscopy (SEM, JEOL JCM 7000, Japan) was utilized to examine the surface morphology of the ZnO material. Before taking SEM, the samples were coated with a thin layer of platinum to enhance conductivity and signal quality, ensuring high-resolution SEM images.

Transmission electron microscopy (TEM, JEOL JEM-1400, Japan) with an accelerating voltage of 100 kV was employed to investigate the morphology and particle size of ZnO nanoparticles.

Ultraviolet-visible spectroscopy (UV-Vis, Shimadzu UV-1900i, Japan) was conducted with a wavelength range from 200 to 1200 nm to determine the maximum absorption wavelength and the optical band gap energy of the material using absorbance spectroscopy.
2.2.3 Assembly of DSSCs and performance measurement
Preparation of the conductive FTO glass: Fluorine-doped tin oxide (FTO) glass substrates (1.5 cm × 1.5 cm) were cleaned using an ultrasonic bath in detergent, acetone, and deionized (DI) water, with each solvent applied for 10 minutes. The cleaned substrates were dried and stored for further use.
Fabrication of the working electrode: A ZnO nanoparticle-based thin film was prepared as follows: 0.1 g of ZnO nanoparticles was mixed with 0.1 mL of ethanol and 0.2 mL of Triton X-100 using an agate mortar and pestle. Subsequently, 0.05 mL of polyethylene glycol (PEG) was added, and the mixture was homogenized. The obtained paste was applied onto the pre-cleaned FTO glass using the doctor blade method to ensure uniform coating. The coated glass was then preheated on a hot plate at 100 °C for 10 minutes, followed by annealing at 400 °C for 60 minutes to enhance adhesion and crystallinity.
Preparation of the natural dye sensitizer: Mangosteen peels were thoroughly washed, dried, and ground into fine powder. One gram of the powdered mangosteen peel was soaked in 10 mL of ethanol and stored in the dark for 24 hours to extract natural pigments. The working electrode was then immersed in this dye solution for 24 hours to allow dye adsorption onto the ZnO surface.
Preparation of the counter electrode: The counter electrode was prepared by depositing a catalytic layer onto the FTO glass. Two types of catalysts were used: (i) Carbon-based catalyst: A carbon layer was deposited onto the FTO glass by rubbing a 2B graphite pencil over the surface. (ii) Platinum-based catalyst: Platinum was sputtered onto the FTO glass using a sputtering system (JEOL, JEC-3000FC, Japan) under 5 kV for 30 seconds.
Preparation of the electrolyte solution: The electrolyte solution was prepared by dissolving 0.127 g of iodine (I2) in 10 mL of ethylene glycol. Then, 0.83 g of potassium iodide (KI) was added to the solution and stirred at room temperature for 30 minutes. The prepared electrolyte was stored in a dark container to prevent degradation.
Assembly and characterization of the solar cell: The DSSC was assembled by sandwiching the working electrode and the counter electrode, with the electrolyte solution injected between them. The assembled solar cells were illuminated using a solar simulator (SAN-EI Electric Japan, XES-40S3) under controlled light conditions. The photovoltaic performance was evaluated by recording the current-voltage (I-V) characteristics using a source meter unit (Keithley 2450, Tektronix). The obtained I-V curves were analyzed to determine key performance parameters, including the efficiency of the solar cells.
3. RESULTS AND DISCUSSION

3.1 Characterization analysis results of ZnO nanoparticles

3.1.1 XRD analysis results of ZnO nanoparticles


[image: image1.emf]20 30 40 50 60 70 80

Intensity (a.u.)

2 theta (degree)

ZnO

JCPDS No79-2205


Figure 1. XRD pattern of ZnO nanoparticles

Figure 1 presents the X-ray diffraction (XRD) pattern of ZnO nanoparticles synthesized via a green synthesis approach using betel leaf extract as a precursor. The XRD analysis was conducted over a 2θ range from 20° to 80°. The characteristic diffraction peaks observed at 2θ values of 31.95º, 34.65º, 36.42º, 47.71º, 56.77º, 63.04º, 68.31º, and 77.7º correspond to the (100), (002), (101), (102), (110), (103), (112), and (201) crystal planes of ZnO, confirming the successful formation of ZnO nanoparticles. The sharpness and intensity of the diffraction peaks indicate a well-defined crystalline structure of the synthesized ZnO nanoparticles.

The average crystallite size of the ZnO nanoparticles (() was determined to be approximately 8.28 nm using the Scherrer equation, which is expressed as follows:
[image: image2.png]_ kx4
T = B coso





Trong đó:

K is the Scherrer constant (typically 0.89 for spherical particles),

λ is the X-ray wavelength (nm),

( is the full width at half maximum (FWHM) of the diffraction peak (radians)

( is the Bragg diffraction angle (degrees).

3.1.2 Band gap energy determination results


[image: image3.emf]300 400 500 600 700 800

Absorbance (a.u.)

Wavelength (nm)

380 nm

ZnO


Figure 2. UV-Vis spectrum of ZnO nanoparticles

To evaluate the optical absorption characteristics of ZnO nanoparticles, the nanoparticles were dispersed in distilled water and subjected to ultrasonication for 15 minutes. The optical absorption properties were then measured using a UV-Vis spectrophotometer, and the results are presented in Figure 2. The obtained spectrum reveals that ZnO nanoparticles exhibit strong absorption in the ultraviolet (UV) region, with a peak absorption wavelength at 380 nm. The bandgap energy (Eg) of the ZnO nanoparticles was calculated using Tauc’s equation [12,13], expressed as
[image: image4.png]



where: max is the wavelength of maximum absorption (nm)

From the plot, the optical bandgap energy (Eg) of the ZnO nanoparticles was determined to be 3.26 eV. This result is consistent with previous studies, confirming the characteristic bandgap energy of ZnO nanoparticles. 
3.1.3 SEM and TEM Analysis of ZnO Nanoparticles

[image: image5.jpg]



Figure 3. SEM images of ZnO nanoparticles at magnifications of (a) 2000×, (b) 5000×, and (c) TEM image of ZnO nanoparticles.

Figure 3 presents the SEM and TEM images of the synthesized ZnO nanoparticles. In Figures 3a and 3b, the SEM images reveal a rough surface morphology; however, the particle shape cannot be distinctly observed at this resolution. SEM imaging is based on the detection and analysis of radiation emitted from the interaction between the electron beam and the material’s surface. Due to the limitations in magnification, the SEM results confirm the nanoscale nature of the material but do not provide clear evidence of spherical particle morphology [14]. To obtain a more detailed assessment of the particle shape and size, TEM analysis was performed, as shown in Figure 3c. The TEM results confirm that the ZnO nanoparticles exhibit a spherical morphology with an average size of 67 nm.
3.2 Results of DSSC efficiency determination


[image: image6.emf]0.0 0.1 0.2 0.3 0.4

0.00

0.05

0.10

0.15

0.20

0.25

0.30

0.35

0.40

Current density 

(

mA/cm

2

)

Voltage (V)

Xúc tác Pt

Xúc tác carbon


Figure 4. J–V curve of DSSC using ZnO nanoparticles as the working electrode with different catalysts.

The J–V characteristic curve of the dye-sensitized solar cell (DSSC) was obtained through photovoltaic measurements using a Tektronix Keithley 2450 instrument, with an active electrode area of 1.0 cm2. As shown in Figure 4, the DSSC employing a Pt catalyst exhibits significantly higher energy conversion efficiency compared to the carbon-based catalyst.

When using a carbon catalyst, the photovoltaic parameters recorded were: an open-circuit voltage (VOC) of 0.21 V, a short-circuit current density (JSC) of 0.117 mA/cm2, a fill factor (FF) of 0.29, and an overall efficiency of 0.007%. In contrast, replacing the carbon catalyst with Pt, while keeping all other parameters unchanged, led to a considerable improvement in DSSC performance. Specifically, VOC increased to 0.41 V, JSC reached 0.61 mA/cm², FF improved to 0.432, and the overall energy conversion efficiency rose to 0.064%. The detailed photovoltaic parameters are summarized in Table 1.

These results highlight the significant enhancement in DSSC performance when using Pt as the catalyst. The VOC of the ZnO-Pt cell (0.41 V) is nearly double that of the ZnO-C cell (0.21 V), while JSC (0.61 mA/cm²) is more than five times higher than that of the ZnO-C cell (0.117 mA/cm²), indicating improved charge transport and electron collection. Furthermore, the increase in FF (from 0.29 to 0.432) contributes to the overall boost in energy conversion efficiency. Consequently, the DSSC with a Pt catalyst achieves an efficiency (η) of 0.064%, which is approximately nine times greater than that of the carbon-based catalyst (0.007%).

The superior catalytic activity of Pt facilitates more efficient redox reactions at the counter electrode, enhancing charge transfer and overall device performance. However, due to the high cost of Pt, further research should focus on developing alternative low-cost catalysts with comparable efficiency to improve the commercial viability of DSSCs.The solar cell efficiency (() is calculated using the following equation:

[image: image7.png]FF X Js¢ X Vo¢

X 100%
P,

n




where:

FF is the fill factor, defined as:

[image: image8.png]pp = Im X Vm

" e X Vo




where: Jm and Vm  are the voltage and current density at the maximum power point, respectively. 

JSC is the short-circuit current density (mA/cm2),

VOC is the open-circuit voltage (V),

Pin is the incident light power per unit area (typically 100 mW/cm2 under standard test conditions)

Table 1. Energy conversion efficiency of DSSC solar cells with different catalysts

	Catalyst
	VOC ( V)
	JSC (mA/cm2)
	FF
	( (%)

	ZnO-C
	0.21
	0.117
	0.29
	0.007

	ZnO-pt
	0.41
	0.61
	0.432
	0.064


Table 2 presents a comparison of the DSSC efficiency obtained in this study with previous research. The results indicate that the efficiency achieved is comparable to some prior studies but remains lower than others. This discrepancy can be attributed to the working electrode made of ZnO, which has not demonstrated high performance due to its relatively large bandgap energy, limiting light absorption and charge transport. To enhance efficiency, further investigation into the impact of different ZnO nanoparticle shapes and sizes on photovoltaic properties is necessary. Additionally, doping ZnO to tailor its bandgap energy to a more favorable range presents a promising approach for improving device performance. 
Table 2. Comparison of solar cell efficiency with previous studies

	Dyes
	η (%)
	Reference

	Spinach (Spinacia oleracea)

Onion (Allium cepa L)

Purple cabbage (Brassica oleracea var capitata ruba)
	0.17

0.064

0.06
	No.27

	Butterfly pea (Clitoria ternatea)
	0.044
	No.28

	Red bean (Vigna angularis)
	0.4
	No.29

	Banana flower (Musa paradisiaca L)
	0.57
	No.30

	Golden shower (Cassia fistula)
	0.21
	No.31

	Mangosteen peel
	0.064
	This study


4. CONCLUSIONS

ZnO nanoparticles were successfully synthesized using betel leaf extract through a simple and environmentally friendly green synthesis method. Characterization techniques, including UV-Vis spectroscopy, XRD, and SEM, confirmed the successful formation of ZnO nanoparticles with an average crystallite size of 8.28 nm and a band gap energy of 3.26 eV. The synthesized ZnO nanoparticles were applied as photoanodes in dye-sensitized solar cells (DSSC). The solar cell achieved an energy conversion efficiency of 0.064% when using a ZnO-based working electrode with a Pt counter electrode.
Acknowledgments

The authors gratefully acknowledge the financial support provided by the Japan Technical Cooperation Project - Phase 2 (TC2) under Grant Model 6.
Conflicts of Interest

The authors declare no conflict of interest.
References

1.
P. K. Nayak, S. Mahesh, H. J. Snaith, D. Cahen. Photovoltaic solar cell technologies: analysing the state of the art, Nature Reviews Materials. 2019, 4(4), 269-285.

2.
I. Massiot, A. Cattoni, S. Collin. Progress and prospects for ultrathin solar cells, Nature Energy. 2020, 5(12), 959-972.

3.
O. Gultepe, F. Atay. Some physical and electrochemical properties of one-dimensional ZnO nanomaterials providing enhanced solar energy harvesting for DSSCs, Materials Letters. 2025, 384(138066.

4.
D.-T. Van-Pham, V. V. Phat, N. T. Q. Hoa, et al. Fabrication of electrospun BaTiO3/chitosan/PVA nanofibers and application for dye-sensitized solar cells, IOP Conference Series: Earth and Environmental Science. 2021, 947(1), 012017.

5.
A. Dutta, M. Nayak, A. J. Akhtar, S. K. Saha. Enhancing photovoltaic efficiency of ZnO based DSSCs through metal ion doping: A comparative simulation study, Journal of Physics and Chemistry of Solids. 2025, 199(112569.

6.
M. Grätzel. Dye-sensitized solar cells, Journal of photochemistry and photobiology C: Photochemistry Reviews. 2003, 4(2), 145-153.

7.
J.-Y. Park, K.-H. Lee, B.-S. Kim, et al. Enhancement of dye-sensitized solar cells using Zr/N-doped TiO 2 composites as photoelectrodes, RSC advances. 2014, 4(20), 9946-9952.

8.
M. Sufyan, U. Mehmood, Y. Qayyum Gill, R. Nazar, A. Ul Haq Khan. Hydrothermally synthesize zinc oxide (ZnO) nanorods as an effective photoanode material for third-generation Dye-sensitized solar cells (DSSCs), Materials Letters. 2021, 297(130017.

9.
W. S. Arsyad, R. Suhardiman, I. Usman, et al. Improvement of Dye-Sensitized Solar Cells (DSSCs) performance using Crude Brazilein Extract from Sappanwood (Caesalpinia Sappan L.) with the incorporation of ZnO nanoparticles, Journal of Molecular Structure. 2024, 1303(137548.

10.
S. Aksoy, K. Gorgun, Y. Caglar, M. Caglar. Effect of loading and standbye time of the organic dye N719 on the photovoltaic performance of ZnO based DSSC, Journal of Molecular Structure. 2019, 1189(181-186.

11.
N. Sarwar, R. Ghaffar, M. Shahzad, et al. Synergistic photovoltaic performance of DSSCs based on ZnO charge transport layers, counter electrodes and C. annuum and T. indica as natural dyes, Materials Science and Engineering: B. 2024, 307(117543.

12.
D.-T. Van-Pham, P. Thi Yen Nhi, T. Vu Bao Long, et al. Electrospun Fe-doped TiO2/chitosan/PVA nanofibers: Preparation and study on photocatalytic and adsorption properties, Materials Letters. 2022, 326(132930.

13.
J. A. Alvarado, G. S. Anaya Conzalez, A. Arce-Plaza, S. Reyes-Carmona. New approach in effective and reproducible green synthesis of pure ZnO nanoparticles using lemon juice with less solvent and without strong base chemical precursor, Ceramics International. 2025, 

14.
H. Hussein, S. S. Ibrahim, S. A. Khairy. Green synthesis of ZnO nanoparticles using Hibiscus sabdariffa L: Rapid Pb2+ ion removal, photocatalytic degradation of methylene blue, and biomedical applications, Journal of Water Process Engineering. 2025, 69(106649.

15.
V. Rafee, A. Razaghizadeh, R. Nakhaei, R. Hosini. Eco-friendly dye-sensitized solar cells: Green synthesis of ZnO nanoparticles using Sargassum algae and performance enhancement through optimized dye combinations, Materials Science and Engineering: B. 2025, 317(118164.

16.
K. Winiarska, M. Klimek-Ochab, Ł. J. Wilk, J. Winiarski. Green synthesis of ZnO nanoparticles using spent coffee extract: Comprehensive characterization and insights, Materials Chemistry and Physics. 2025, 338(130621.

17.
D. E. Yizengaw, E. M. Godie, A. H. Manayia. Green synthesis and characterization of ZnO nanoparticles using Justicia Schemperiana leaf extract and its antibacterial and antioxidant activity, Inorganic Chemistry Communications. 2025, 174(114071.

18.
Z. U. Zango, A. Garba, F. B. Shittu, et al. A state-of-the-art review on green synthesis and modifications of ZnO nanoparticles for organic pollutants decomposition and CO2 conversion, Journal of Hazardous Materials Advances. 2025, 17(100588.

19.
C.-H. Lu, C.-H. Yeh. Influence of hydrothermal conditions on the morphology and particle size of zinc oxide powder, Ceramics International. 2000, 26(4), 351-357.

20.
S.-C. Liu, J.-J. Wu. Low-temperature and catalyst-free synthesis of well-aligned ZnO nanorods on Si (100), Journal of Materials Chemistry. 2002, 12(10), 3125-3129.

21.
Y.-L. Wei, P.-C. Chang. Characteristics of nano zinc oxide synthesized under ultrasonic condition, Journal of Physics and Chemistry of Solids. 2008, 69(2-3), 688-692.

22.
Y. Wang, C. Zhang, S. Bi, G. Luo. Preparation of ZnO nanoparticles using the direct precipitation method in a membrane dispersion micro-structured reactor, Powder Technology. 2010, 202(1-3), 130-136.

23.
S. Das, R. Parida, I. Sriram Sandeep, S. Nayak, S. Mohanty. Biotechnological intervention in betelvine (Piper betle L.): A review on recent advances and future prospects, Asian Pacific Journal of Tropical Medicine. 2016, 9(10), 938-946.

24.
R. K. Gupta, P. Guha, P. P. Srivastav. Phytochemical and biological studies of betel leaf (Piper betle L.): Review on paradigm and its potential benefits in human health, Acta Ecologica Sinica. 2023, 43(5), 721-732.

25.
T. Singh, P. Singh, V. K. Pandey, R. Singh, A. H. Dar. A literature review on bioactive properties of betel leaf (Piper betel L.) and its applications in food industry, Food Chemistry Advances. 2023, 3(100536.

26.
V. T. Tran, T. B. Nguyen, H. C. Nguyen, N. H. N. Do, P. K. Le. Recent applications of natural bioactive compounds from Piper betle (L.) leaves in food preservation, Food Control. 2023, 154(110026.

27.
A. M. Ammar, H. S. H. Mohamed, M. M. K. Yousef, G. M. Abdel-Hafez, A. S. Hassanien, A. S. G. Khalil. Dye-Sensitized Solar Cells (DSSCs) Based on Extracted Natural Dyes, Journal of Nanomaterials. 2019, 2019(1), 1867271.

28.
H. Karimah, W. M. I. W. Ismail, A. Ali. The electrical conductivity properties of Morus Nigra L. sp., Clitoria ternatea sp., and Melastoma malabathricum L. sp. as natural photo-sensitizers, AIP Conference Proceedings. 2019, 2068(1), 

29.
Rahul, P. K. Singh, B. Bhattacharya, Z. H. Khan. Environment approachable dye sensitized solar cell using abundant natural pigment based dyes with solid polymer electrolyte, Optik. 2018, 165(186-194.

30.
W. A. Dhafina, H. Salleh, M. Z. Daud, M. S. M. Ghazali. Low cost dye-sensitized solar cells based on zinc oxide and natural anthocyanin dye from Ardisia elliptica fruits, Optik. 2018, 172(28-34.

31.
I. Chandra Maurya, S. Singh, P. Srivastava, B. Maiti, L. Bahadur. Natural dye extract from Cassia fistula and its application in dye-sensitized solar cell: Experimental and density functional theory studies, Optical Materials. 2019, 90(273-280.




Corresponding author: Doan Van Hong Thien
Faculty of Chemical Engineering, Can Tho University
3/2 Street, Ninh Kieu District, Can Tho City, Vietnam
Email: dvhthien@ctu.edu.vn, 
Tel: +84-944551337, 
ORCID: 0000-0003-3023-6148
9

_1803292081.bin

_1803292082.bin

_1803292080.bin

