
Tổng hợp Co3O4 từ tiền chất ZIF-67 và ứng dụng biến tính điện cực phát hiện acid ascorbic

Ngô Thị Thanh Hiền1,*, Nguyễn Vũ Ngọc Mai1

1Khoa Khoa học tự nhiên, Trường Đại học Quy Nhơn, Việt Nam

*Tác giả liên hệ chính. Email: ngothanhhien@qnu.edu.vn

Ngày nhận bài: dd/mm/yy; Ngày sửa bài: dd/mm/yy

Ngày nhận đăng: dd/mm/yy; Ngày xuất bản: dd/mm/yy

TÓM TẮT

Trong nghiên cứu này, Co3O4 dạng tinh thể có cấu trúc xốp được tổng hợp bằng cách nung ZIF-67 trong môi trường không khí. Đặc trưng vật liệu Co3O4 được nghiên cứu bằng XRD, BET, SEM và EDS. Điện cực biến tính Co3O4-GPE dùng phát hiện điện hóa acid ascorbic thể hiện khoảng tuyến tính từ 2 µM đến 15 µM với giới hạn phát hiện là 0,48 µM. Kết quả độ thu hồi dao động từ 97,82% đến 99,5% đối với acid ascorbic xác định trong viên thuốc thương mại.
Từ khoá: Co3O4, ZIF-67, acid ascorbic. 
ZIF-67-derived Co3O4 Porous Crystalline Material for The Electrochemical Detection of Ascorbic Acid
Ngo Thi Thanh Hien1*, Nguyen Vu Ngoc Mai1
1Faculty of Natural Sciences, Quy Nhon University, Vietnam
*Corresponding author. Email: ngothanhhien@qnu.edu.vn

Received: dd/mm/yyyy; Revised: dd/mm/yyyy;

Accepted: dd/mm/yyyy; Published: dd/mm/yyyy

ABSTRACT

The Co3O4 porous crystalline material was synthesized through the calcination of ZIF-67 sample in air atmosphere. The Co3O4 material was characterized by XRD, BET, SEM, and EDS. The electrode modified with Co3O4 was used for the determination of ascorbic acid. The proposed Co3O4-GPE electrode exhibited a linear range of 2 µM to 15 µM with a detection limit of 0.48 µM. Recovery results, ranging from 97.82% to 99.5%. for ascorbic acid in pharmaceutical tablet.

Keywords: Co3O4, ZIF-67, ascorbic acid.
1. INTRODUCTION 
Vitamin C, also known as ascorbic acid (AA), is a common ingredient in multivitamins and is found naturally in many foods. It is important for a healthy diet and acts as an antioxidant. However, an overdose of vitamin C can lead to side effects such as stomach upset, headache, difficulty sleeping, and skin flushing.1,2 Therefore, the rapid and accurate determination of AA has attracted scientific attention.

Numerous analytical methodologies have been reported for the determination of ascorbic acid (AA), including techniques such as spectrofluorometry,3,4 chromatography,5,6 spectrophotometry,7,8 capillary zone electrophoresis,9,10 and electrochemistry11,12. Among these, electrochemical methods utilizing modified electrodes have attracted considerable interest due to their inherent simplicity, high sensitivity, and cost-effectiveness.
Cobalt oxide is a semiconductor with wide applications in many fields, including catalysis, electrode materials, gas sensing, and drug delivery.13-15 Numerous studies have explored the diverse applications of Co₃O₄; however, its potential use in electrode modification for pharmaceutical analysis remains relatively underexplored. To date, various porous nanostructures of Co₃O₄ have been synthesized, including spherical, tubular, rod-like, and flower-like morphologies. Most synthesis methods utilize cobalt carbonate or hydroxide salts as precursors, often yielding materials with relatively low surface areas.16,17
Recent, the application of metal-organic frameworks (MOFs; ZIFs) as precursors in the synthesis of inorganic materials is a growing area of research.18-25 Studies show that heat treatment of ZIF-67 can pyrolyze their ligands and lead to the formation of metal oxide nanoparticles. Therefore, the metal-centered organic framework material Co (ZIF-67) has appeared as a potential precursor to synthesize cobalt oxide (Co3O4) while still inheriting the structural characteristics of ZIF-67 and improving its catalytic activity. 

In this work, an electrode modified with the Co3O4 porous crystalline material derived from ZIF-67 is demonstrated. The obtained electrode was used for the electrochemical determination of AA.
2. EXPERIMENT

2.1. Chemicals

2-methylimidazol  (2-Hmim, 98.0%), ascorbic acid, graphite powder and parafin oil were received from Sigma Aldrich. Cobalt nitrate hexahydrate [Co(NO3)2·6H2O, 99.0%] was purchased from Macklin (China). Phosphoric acid (H3PO4, 85%), potassium dihydrogen phosphate (KH2PO4, 99%), boric acid (H3BO3, 99%)  and potassium hydroxide (KOH)  were purchased from Guangdong- Guanghua Sci-Tech Co. Ltd (China).

 Vitamin C tablet (Vitamin C, 500 mg AA, from Pharimexco Viet Nam) was purchased from a local pharmacy. All chemical reagents were used as received without any further purification. And all aqueous solution were prepared with distilled water.

The Britton–Robinson (B-R) buffer solutions were prepared from 0.5 M H3BO3, 0.5 M H3PO4, and 0.5 M CH3COOH solutions. The desired pH of the B–R buffer was adjusted using 1 M KOH or 1 M H3PO4 solutions.

2.2. Apparatus

All electrochemical measurements (cyclic voltammetry and square wave voltammetry) were carried out at the DY2322  potentiostat made by Digi-Ivy, Inc. Austin. A conventional three-electrodes cell equipped with a working electrode (Co3O4-GPE modified electrode or GPE unmodified electrode, with a geometrical area of 0.07 cm2), a counter electrode (Pt wire), and a reference electrode (Ag/AgCl, KClsat) was used. 
2.3 Synthesis of Co3O4 porous crystalline material from ZIF-67

ZIF-67 was synthesized according to the previously reported method26. 
1.455 g of Co(NO3)2⋅6H2O was dissolved in 50 mL of ethanol and 1.64 g of 2-methylimidazole (Hmim) was dissolved in 50mL of ethanol. Mole ratio of Co2+: Hmim was 1 : 4. The Hmim solution was poured slowly into Co(NO3)2⋅6H2O solution under stirring condition for 30 min at room temperature. The obtained solution was kept at room temperature for 6 hours without stirring. The colloidal dispersion was observed, and the product was collected by centrifugation (4000 rpm, 30 min) and washed with ethanol three times, then dried at 80 oC, 12 hours.
Co3O4 was obtained through the calcination of ZIF-67 in air atmosphere with a heating rate of 1 °C·min−1.

2.4. Preparation of Co3O4-GPE modified electrode

The Co3O4-GPE modified electrode was prepared by thoroughly mixing 40 mg of graphite powder and 5 mg Co3O4 powder with 10 μL of paraffin oil. The obtained paste was put into the cavity of a Teflon holder. The obtained electrode surface was smoothed using paper. When necessary, a new electrode surface was obtained by removing 2 mm of the outer paste layer and adding freshly modified paste.
2.5. Characterization of the Co3O4 porous crystalline material

The powder X-ray diffraction (XRD) data was performed on Bruker-AxsD8 diffractometer under 40kV and 40mA. Textural characteristics of sample was determined from the adsorption – desorption isotherms of nitrogen at -196 oC using a Gemini VII 2390 V1.02 Micromeritics automated instrument.  Scanning electron microscope (SEM) was performed on a JEOL JSM-6700F field emission SEM, which was operated at the accelerating voltage of 15 kV and the detector current of 10 mA. EDS analysis was recorded by using a JSM-5700 LV.

3. RESULTS AND DISCUSSION

3.1. Characterization of the synthesized Co3O4 material

The XRD diffraction pattern of Co3O4 sample are shown in Fig. 1. X-ray diffraction pattern exhibited reflections at 2θ values of approximately 31.5°, 36.8°, 38.0°, 44.6°, 55.8°, 59.4°, 65.3° and 77.5°, corresponding to the (220), (311), (222), (400), (422), (511), (440) and (533) crystalline planes of the Co3O4 cubic structure (JCPDS No. 04-043-1003)25.
[image: image23.png]IMS-NKL 5.0kV 5.2mm x20.0k SE(M




Figure 1. XRD pattern of the Co3O4 porous crystalline material.

Nitrogen adsorption-desorption isotherms were employed to characterize the specific surface area and pore morphology of the Co3O4 sample. As depicted in Figure 2, the sample presented a Type IV isotherm, accompanied by an H3 hysteresis loop, suggesting a mesoporous structure. The BET surface area was determined to be 30.43 m²/g, and the pore size distribution was at 3 nm.


[image: image2]
Figure 2. Nitrogen adsorption−desorption isotherms (A) and pore size distribution (B) of the Co3O4 porous crystalline material.


[image: image3]
Figure 3. SEM image of the Co3O4 porous crystalline material, Inset: SEM image of ZIF-67 material.
[image: image1.emf]Meas. data:Co3O4-ZIF67-350

Intensity (cps)

          0

       1000

       2000

       3000

       4000

       5000

2-theta (deg)

20 30 40 50 60 70 80

Cobalt Oxide, Co3 O4, 00-043-1003

[image: image9.png]o
©

o
N~
(d

_
o o o o (=] o
© wn < (2] N -~

LS B/.wd) paqiospy Auenp

o

04 0.6 0.8 1.0
Relative Pressure (p/p°)

0.2

0.0



[image: image10.png]20

N
-

°
(

wu.-Bj,w) eary aiod Ap/vpP

Pore Diameter (nm)



[image: image11.png]


[image: image12.png]


SEM images of Co3O4 (Figure 3) revealed that the calcined particles retained a cubic morphology, consistent with the original ZIF-67 crystal template, characterized by an internal hollow structure and a surface exhibiting porosity. However, thermal treatment resulted in the observation of some collapsed hollow structures.
[image: image13.png]]





[image: image4]
Figure 4. EDS spectra of the Co3O4 porous crystalline material.

EDS analysis was conducted on the Co3O4 sample (Figure 4). The results confirmed the presence of cobalt (Co) and oxygen (O) elements on the sample's surface. Elemental analysis of the Co3O4 yielded 41.62% cobalt and 58.38% oxygen.

A comprehensive morpho-structural analysis of the Co3O4 material, utilizing X-ray diffraction (XRD), scanning electron microscopy coupled with energy-dispersive X-ray spectroscopy (SEM-EDS) and nitrogen adsorption-desorption isotherm, validated the successful synthesis of the Co3O4 porous crystalline material.

3.2. Electrochemical characterization

The electrochemical behavior of ascorbic acid (AA) was investigated using cyclic voltammetry (CV) and square wave voltammetry (SWV). 
[image: image14.png]e |

ok
o

Toats

W

s

1000

o

ey
s




[image: image5]
Figure 5. Cyclic voltammograms (A) and square wave voltammograms (B) at GPE and Co3O4-GPE modified electrode in  0.2 M B-R buffer solution pH = 4 containing an concentration of 10-4 M AA.

A peak of AA at 0.08 V was observed in the CV and SWV curves obtained at both the bare GPE and the Co3O4-GPE, as illustrated in Figure 5. The Co3O4-GPE exhibited a lower peak potential and higher current. The oxidation peak current for AA at the Co3O4-GPE was approximately fifteen-fold greater than that observed at the bare GPE (Figure 5B) . This enhancement is attributed to the increased surface area, porous morphology, and functional properties of the Co3O4 modification compared to the bare GPE.
3.3. The effect of pH

The effect of pH on the voltammetric signals of AA was studied in the pH range of 3 to 6 using square wave voltammetry (SWV). The pH of the electrolyte significantly affects the AA oxidation on the modified electrode. Figure 6 displays the current responses recorded on the Co3O4-GPE under different pH conditions.
A substantial increase in peak current was observed as tacc increased from 0 to 90 seconds, suggesting a corresponding enhancement of AA accumulation at the electrode surface. Beyond 90 seconds, however, the peak current exhibited negligible increase, indicative of the electrode surface approaching adsorption equilibrium. Based on this observation, 90 seconds was selected as the optimal tacc.
3.4. Accommulation

The effect of accumulation time (tacc) on electrode response was investigated across a range of 0 to 150 seconds in a 0.2 M B-R buffer solution (pH 4) containing 10-4 M AA (Figure 7).

[image: image6]
Figure 6. Square wave voltammograms of Co3O4-GPE in 0.2 M B–R buffer solution pH 4 containing 10−4 M AA (A); Influence of pH on peak current (B); linear plot of Ep vs. pH (C).

[image: image7.png]


 
Figure 7. Dependence of Ip for AA in 0.2M B-R buffer solution pH 4 on accummulation time.
3.5. Calibration

The calibration curves for the AA detection with varying concentrations of AA was constructed by recording SWV in 0.2 M B-R  buffer solution at pH = 4 (Figure 8A).  Accordingly, a calibration curve was shown in Figure 8B.  The electrode exhibited a linear response for AA concentrations between 2 µM and 15 µM.


[image: image8]
Figure 8. Square wave voltammograms recorded at Co3O4-GPE increasing concentration of AA (A) and the corresponding calibration curve (B).
The linear regression equation was as follow:

Ipa/μA = (-3.56335 ± 0.19192) + (1.19706 ± 0.02218) [AA]/μM,    (R = 0.99726)

The Co3O4-GPE electrode achieved a detection limit of 0.48 µM and a sensitivity of 1.19 for ascorbic acid (AA) determination. The obtained results are lower comparatively with some reported in the literature 1.52 µM at CL-TiN/GCE,27 0.5 µM atNiCoO2/C,28 0.83 µM at AgNP-Psi29.

4. REAL SAMPLE ANALYSIS
To evaluate the applicability of the Co3O4-GPE for real sample analysis, the Co3O4-GPE was employed for the analysis of ascorbic acid in Vitamin C tablet (Pharimexco Viet Nam) using the standard addition method. The results, summarized in Table 1, confirm the electrode's efficacy for AA determination in pharmaceutical formulations. The measured mean AA concentration demonstrated agreement with the labeled value, and recovery rates ranged from 97.82% to 99.5%.

Table 1. Results of real sample analysis
	Sample
	Added (µM)
	Found (µM)
	Recovery (%)
	RSD (%)

	Vitamin C  (500 mg)
	3
	2.96 ± 0.02
	98.66 ± 0.84
	0.85


5. CONCLUSION
The synthesis of Co3O4 porous crystalline material was performed using the ZIF-67 material as a precursor. The resulting Co3O4 possesses an internal hollow structure and a surface exhibiting porosity. The Co3O4-GPE porous crystalline material were used to develop a modified electrode, which demonstrates promise for AA detection due to its high sensitivity, and low detection limit. The Co3O4-GPE was successfully used for the determination of ascorbic acid in real samples.

ACKNOWLEDGEMENTS 

This research is conducted within the framework of Science and Technology Projects at institutional level of Quy Nhon University under the project code T2024.832.03. 

REFERENCES

1.    M. Levine, Y. Wang, S.J. Padayatty, J. Morrow, A new recommended dietary allowance of vitamin C for healthy young women, Proceeding of the National Academy of Science, 2001, 98, 9842–9846.

2.   C.M. Nam, K.W. Oh, K.H. Lee, S.H. Jee, S.Y. Cho, W.H. Shim, I. Suh, Vitamin C intake and risk of ischemic heart disease in a population with a high prevalence of smoking, Journal of the American College of Nutrition, 2003, 22, 372–378.

3.   A. Jain, A. Chaurasia, K.K. Verma, Determination of ascorbic acid in soft drinks, preserved fruit juices and pharmaceuticals by flow injection spectrophotometry: matrix absorbance correction by treatment with sodium hydroxide, Talanta, 1995, 42, 779–787. 

4. M. Tabata, H. Morita, Spectrophotometric determination of a nanomolar amount of ascorbic acid using its catalytic effect on copper(II) porphyrin formation, Talanta, 1997, 44, 151–157.

5.    J. Lykkesfeldt, Determination of ascorbic acid and dehydroascorbic acid in biological samples by high-performance liquid chromatography using subtraction methods: reliable reduction with tris [2-carboxyethyl] phosphine hydrochloride,  Analytical Biochemistry, 2000, 282, 89–93.

 6.  R. Thomis, E. Roets, and J. Hoogmartens, Analysis of tablets containing aspirin, acetaminophen, and ascorbic acid by high-performance liquid chromatography, Journal of Pharmaceutical Sciences, 1984,  73,  1830–1833.

7.   P. Ortega Barrales, M. L. Fernández de Córdova, and A. Molina Dıaz, Indirect determination of ascorbic acid by solid-phase spectrophotometry, Analytica Chimica Acta, 1998, 360, 143–152.

8. M. Tabata, H. Morita, Spectrophotometric determination of a nanomolar amount of ascorbic acid using its catalytic effect on copper(II) porphyrin formation, Talanta, 1997, 44, 151–157 

9.   W.S. Law, P. Kubáň, J.H. Zhao, S.F.Y. Li, P.C. Hauser, Determination of vitamin C and preservatives in beverages by conventional capillary electrophoresis and microchip electrophoresis with capacitively coupled contactless conductivity detection, Electrophoresis, 2005, 26, 4648–4655. 

10.  T. Wu, Y. Guan, J. Ye, Determination of flavonoids and ascorbic acid in grapefruit peel and juice by capillary electrophoresis with electrochemical detection, Food Chemistry, 2007,  100, 1573–1579.

11. Yuhong Zheng, Huaiwei Zhang & Li Fu, Preparation gold nanoparticles using herb leaf extract for electro-oxidation determination of ascorbic acid, Inorganic and Nano-Metal Chemistry, 2018, 48, 449-453.

12.  A Pardakhtya, S Ahmadzadeha, S Avazpoura, V K Gupta, Highly sensitive and efficient voltammetric determination of ascorbic acid in food and pharmaceutical samples from aqueous solutions based on nanostructure carbon paste electrode as a sensor, Journal of Molecular Liquids, 2016, 216, 387–391.

13.  Chen X., Cheng J., Shou Q., Liu F., Zhang X, Effect of calcination temperature on the porous structure of cobalt oxide micro-flowers, CrystEngComm, 2012, 14, 1271-1276 

 14. Sun C., Rajasekhara S., Chen Y., Goodenough J.B, Facile synthesis of monodisperse porous Co3O4 microspheres with superior ethanol sensing properties, Chemical Communications, 2011, 48,  12852-12854. 

15.  Sun C., Su X., Xiao F., Niu C., Wang J, Synthesis of nearly monodisperse Co3O4 nanocubes via a microwave-assisted solvothermal process and their gas sensing properties, Sensors and Actuators B: Chemical, 2011, 157,  681-685. 

16. R. He, H. Liang, C. Li, J. Bai, Enhanced photocatalytic hydrogen production over Co3O4@g-C3N4 p-n junction adhering on one-dimensional carbon fiber, Colloids and Surface A: Physicochemical and Engineering Aspects,  2020, 586, 124200.

17.  H. Yu, J. Xu, Z. Liu, Functionalization of sheet structure MoS2 with CeO2–Co3O4 for efficient photocatalytic hydrogen evolution, Jounal of Materials Science, 2018, 53, 15271–15284.

18.  Y.-Y. Zheng; C.-X. Li; X.-T. Ding; Q. Yang; Y.-M. Qi; H.-M. Zhang; L.-T. Qu; Chin, Continuous synthesis for zirconium metal-organic frameworks with high quality and productivity via microdroplet flow reaction, Chemistry Letters, 2017, 28, 1473–1478 

 19.  M.Z. Hussain, Z. Yang, Z. Huang, Q. Jia, Y. Zhu, Y. Xia, Recent advances in metal–organic frameworks derived nanocomposites for photocatalytic applications in energy and environment, Advanced Science, 2021,  14, 2100625. 

20.  W. Li, X. Wu, N. Han, J. Chen, X. Qian, Y. Deng, W. Tang, Y. Chen, MOF-derived
hierarchical hollow ZnO nanocages with enhanced low-concentration VOCs gas sensing performance, Sensors and Actuators B: Chemical, 2016, 225, 158–166. 

21.  K. Tao, X. Han, Q. Yin, D. Wang, L. Han, L. Chen, Metal-organic frameworks derived porous In2O3 hollow nanorod for high-performance ethanol gas sensor, ChemistrySelect, 2017, 33, 10918–10925.

22.   Y. Cai, G. Fang, J. Zhou, S. Liu, Z. Luo, A. Pan, G. Cao, S. Liang, Metal -organic
framework -derived porous shuttle-like vanadium oxides for sodium-ion battery application, Nano Research, 2018, 11, 449–463.  

23.  M.H. Yap, K.L. Fow, G.Z. Chen, Synthesis and applications of MOF-derived porous
nanostructures, Green Energy & Environment, 2017, 3, 218–245 

24. C. Zhang, W. Chu, · R. Jiang · L. Li · Q. Yang, · Y. Cao, J. Yan, ZIF‑67, Derived Hollow Structured Co3O4 Nanocatalysts: Tunable Synthetic Strategy Induced Enhanced Catalytic Performance, Catalysis Letters, 2019, 149,  3058–3065.

25. X. Yan, L. Tian, M. He, X. Chen, Three-Dimensional Crystalline/Amorphous Co/Co3O4 Core/Shell Nanosheets as Efficient Electrocatalysts for the Hydrogen Evolution Reaction, Nano Letters Journal, 2015, 15, 6015-6021.

26.  Thi Thanh Hien Ngo, Thi Hai Yen Pham, Nguyen Thoai Dang, Thi Vuong Hoan Nguyen, Thanh Huyen Pham, Graziella Liana Turdean, Graphite paste electrode modified with zeolitic imidazolate framwork (ZIF-67) for the determination of acetaminophen, Studia UBB Chemia, 2023, 1, 7-17. 

27.  L. Zhang, J. Feng, K.-C. Chou, L. Su, X. Hou, Simultaneously electrochemical detection of uric acid and ascorbic acid using glassy carbon electrode modified with chrysanthemum-like titanium nitride, Journal of Electroanalytical Chemistry, 2017, 803, 11–18.

28.  X. Zhang, S. Yu, W. He, H. Uyama, Q. Xie, L. Zhang, F. Yang, Electrochemical sensor based on carbon-supported NiCoO2 nanoparticles for selective detection of ascorbic acid, Biosensors and Bioelectronics, 2014, 55, 446–451.

29. F.A. Harraz, M. Faisal, A.E. Al-Salami, A.M.   El-Toni, A.A. Almadiy, S.A. Al-Sayari, M.S. Al-Assiri, Silver nanoparticles decorated stain-etched mesoporous silicon for sensitive, selective detection of ascorbic acid, Materials Letters, 2019, 234, 96–100.

.

(B)








[image: image15.png]002

02,

004

206,

A)

oopeerenotun]

oot

e

<z

o0

Ev

0z o4 os



[image: image16.png]™

e

®)

—cospuares whums

o1

00

o1 0z

03



[image: image17.png]o cind

@A

v

0



[image: image18.png]B




[image: image19.png]o0

005,

o0

©




[image: image20.png]L

ho v b o

1.

n
0




[image: image21.png]™

wl (B)



[image: image22.png]‘Spectrum 1

o

co




