GIẢI TRÌNH, BỔ SUNG, CHỈNH SỬA BÀI BÁO

Tên bài báo

Study on dispersion of SiO2/g-C3N4 on polyvinylidene fluoride substrate and photocatalytic activity in decomposing RhB solution in aqueous environment

Căn cứ vào nhận xét phản biện, thay mặt nhóm tác giả xin gửi bản giải trình, bổ sung, chỉnh sửa bài báo như sau:

| TT | Nội dung nhận xét của phản biện | Giải trình, chỉnh sửa, bổ sung của nhóm tác giả |
| --- | --- | --- |
|  | Phản biện 1 |  |
| 1 | In sections 2.2.1, 2.2.2, 2.2.3, and 2.2.4, the majority of sentences lack subjects. The complete sentences should be rewritten. | Thank you for your comment. The authors have edited and yellow-highlighted sections 2.2.1, 2.2.2, 2.2.3, and 2.2.4 of the article. |
| 2 | There are some errors of extra/missing spaces. The author is requested to double-check. | Thanks for your suggestion. The authors have checked and corrected some errors in the extra/missing spaces in the article. |
| 3 | To demonstrate the novelty of this work, the author can discuss and evaluate a few specific related research studies in the introduction. | Thank you for your comment. The authors have demonstrated, discussed, evaluated, and highlighted the novelty of a few specific related research studies in the introduction of this work. |
| 4 | It is necessary to compare the research findings with those of previous studies, especially the results related to decomposition efficiency. | Thanks for your suggestion. A comparison of the rate constant of the present work with the previous works is listed in Table S1. However, the comparison is lame because the reaction conditions are not the same. However, Table S1 shows that the rate constant of SiO2/g-C3N4/PVDF is relatively high compared to previous studies. |
| 5 | The author should think about including more references, as there are now only 13 references in the manuscript. | Thank you for your comment. The authors added additional references to the article from 13 references to 24 references. |
|  | Phản biện 2 |  |
| 1 | In the introduction section, the logic of thinking in introducing the background and purpose of the study is not clear enough; please provide more knowledge on the significance of the study. The following references are suggested to cite: [1] Long, P. B. B., Nguyen, V. C., Le Pham, H. A., Dang, H. P. (2025). Effect of the Dimethylformamide/Isopropanol Solvent Ratio on the Structure, Optical Properties, and Photodegradation Performance of RhB Using Bi-MOF. Bulletin of Chemical Reaction Engineering & Catalysis, 20(1), 166-176. [2] Ta, Q. T. H., Namgung, G., & Noh, J. S. (2019). Facile synthesis of porous metal-doped ZnO/g-C3N4 composites for highly efficient photocatalysts. Journal of Photochemistry and Photobiology A: Chemistry, 368, 110-119. | Thank you for your comment. The authors have added these two references to the introduction of the article. |
| 2 | It is suggested that the author use a table to compare the results of the material in this paper with the previous works. | Thanks for your suggestion. A comparison of the rate constant of the present work with the previous works is listed in Table S1. However, the comparison is lame because the reaction conditions are different. However, Table S1 shows that the rate constant of SiO2/g-C3N4/PVDF is relatively high compared to previous studies. |
| 3 | Figure 3: Please provide the size of SiO2. | Thanks for your suggestion. The average size of the SiO₂ particles in Figure 3 is 30–50 nm on the ruler's scale. |
| 4 | What are the final products after rhodamine B (RhB) degradation? | Thanks to you for your suggestion. After rhodamine B (RhB) degradation, the final products typically include small organic molecules. |
| 5 | The improved mechanism of the Photodegradation is insufficient; please provide more details in the band edge diagram. | Thank you for your comment. We have revised as follows: Based on the above results, the photocatalytic mechanisms for the g-C3N4/SiO2/PVDF fibers under visible light are tentatively proposed, and illustrated in Fig. S1. g-C3N4 + hν → g-C3N4 (e- + h+) (1) O2 + e- → O2- (2) O2- + 2H+ + e → H2O2 (3) O2- + H2O2 → OH + HO- + O2 (4) (OH/O2-/h+) + RhB → Degradation products (5) Upon exposure to visible light, g-C₃N₄ in the g-C₃N₄/SiO₂/PVDF composite absorbs photons and generates electron–hole pairs (e⁻/h⁺). Due to its low electrical conductivity, the photocatalytic reactions mainly occur on the surface of g-C₃N₄. + The photogenerated electrons (e⁻) in the conduction band of g-C₃N₄ are transferred to oxygen molecules (O₂) near the surface, reducing them to superoxide radicals (·O₂⁻). These ·O₂⁻ radicals are potent oxidizing agents, capable of degrading the dye RhB. + The remaining holes (h⁺) in the valence band (VB) of g-C₃N₄ also directly participate in the oxidation of RhB, further assisting in the degradation of the pollutant.1 1. Meng-Jie Chang, Wen-Na Cui, Jun Liu, Kang Wang, Xiao-Jiao Chai, "Fabrication and photocatalytic properties of flexible g-C3N4/SiO2 composite membrane by electrospinning method", Journal of Materials Science: Materials in Electronics, 2018. |

Table S1: Comparison of the rate constant of the present catalyst with published papers.

[1]	Z. Vilamova et al., "Fibrous PVDF membranes modified by anchored g-C3N4@ GO composite with enhanced photocatalytic activity," Applied Surface Science, vol. 677, p. 161055, 2024.

[2]	Z. Vilamova et al., "Enhancing photocatalytic g-C3N4/PVDF membranes through new insights into the preparation methods," Polymer, vol. 307, p. 127238, 2024.

[3]	R. Liu et al., "Synthesis and characterization of g-C3N4/Ag3PO4/TiO2/PVDF membrane with remarkable self-cleaning properties for rhodamine B removal," International Journal of Environmental Research and Public Health, vol. 19, no. 23, p. 15551, 2022.

[4]	T.-T. Zhou et al., "Flexible TiO2/PVDF/g-C3N4 nanocomposite with excellent light photocatalytic performance," Polymers, vol. 12, no. 1, p. 55, 2019.

Xin trân trọng cảm ơn!

Ngày 28 tháng 08  năm 2025

TM NHÓM TÁC GIẢ

Nguyễn Thị Lan